Supplementary Material

Text. S1 Characterizations

Total sugar content in penicillin fermentation residues (PR) was measured by the phenol-sulfuric acid colorimetric method. Crude protein content in PR was measured by the Kjeldahl method. Crude fat content in PR was measured by the Soxhlet extraction method.

High-performance liquid chromatography-mass spectrometry (HPLC-MS; Agilent 6410B, USA) was used to determine antibiotic residues in biochar.

Text. S2 Batch experiments

To study the desorption of biochar, NaOH, HCl, and CH₃OH were applied. 0.03 g of adsorbed saturated biochar sample was added to 40 ml of 1 mol/L solution of HCl, NaOH and CH₃OH, respectively. The flasks were shaken at 25℃ at 200 rpm for 2 h. Then, the samples were filtered through a 0.45 µm membrane and investigated by a spectrophotometer to calculate the desorption amount.

To study the renewability of biochar, the NaOH method, the hot alkaline method, and the UV/H2O2 regeneration method were applied. NaOH method: 0.03 g of adsorption-saturated biochar sample was placed in 40 mL of NaOH solution with a concentration of 1 mol/L, shaken at 25℃ and 200 rpm for 2 h to complete a regeneration, followed by drying the sample for the next cycle of the adsorption experiment. Hot alkali method: 0.1 g of adsorption-saturated biochar sample was placed in 40 mL of NaOH solution with a concentration of 1 mol/L at 55℃ and shaken at 200 rpm for 2 h to complete a regeneration, followed by drying the sample for the next cycle of the adsorption experiment. UV/H2O2 regeneration method: 0.1 g of adsorption-saturated biochar sample was placed in 40 mL of H2O2 (5 wt%) solution, with UV lamp irradiation, and shaken at 25℃ and 200 rpm for 2 h to complete the regeneration, followed by drying the sample for the next cycle of the adsorption experiment.

Text. S3 Desorption and recycle performance

The desorption ability of IKBCH was shown in Table S1. The cycling performance of IKBCH was shown in Figure S2.

Text. S4 Environmental impact and economic feasibility

Antibiotic residues in biochar measured by HPLC. The results were shown in Table S3.

Table S1 List of kinetic and isotherm models

| Models | Expressions |
| --- | --- |
| Pseudo-first-order | qt=qe1-e-k1t |
| Pseudo-second-order | qt=qe2k2t1+qek2t |
| Intraparticle diffusion | qt=kdit1/2+C |
| Langmuir | qe=qmKLce1+KLce |
| Freundlich | qe=KFce1/n |

Where qe (mg/g) is the adsorbed amount of TC at equilibrium, qt (mg/g) is the adsorbed amount of TC at time t. k1 is the rate constant for the pseudo-first-order (1/h), k2 is the rate constant for the pseudo-second-order (g/mg·h), and kdi is the rate constant for the intraparticle diffusion (mg/g·h1/2) rate constant. ce (mg/L) is the TC concentration at equilibrium, qm (mg/g) is the Langmuir maximum capacity, KL (L/mg) is the Langmuir constant, KF (mg/g) is the Freundlich adsorption capacity, and n is the adsorption intensity.

Table S2 Adsorption parameters of TC adsorption isotherm model

| Temperature | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qm | KL | R2 | 1/n | KF | R2 |
| 25℃ | 268.5516 | 11.7133 | 0.9999 | 0.0549 | 219.4036 | 0.8602 |
| 35℃ | 281.5401 | 29.7432 | 0.9999 | 0.0531 | 234.7635 | 0.8161 |
| 45℃ | 291.1798 | 26.6277 | 0.9978 | 0.0549 | 243.2564 | 0.6262 |

Table S3 The desorption ability of IKBCH.

| Desorption method | Desorption capacity (mg/g) |
| --- | --- |
| NaOH | 86.02 |
| HCl | 9.84 |
| CH₃OH | 12.43 |

Table S4 Antibiotic concentration (ng/L).

| Penicillin types | Sample 1 | Sample 2 |
| --- | --- | --- |
| Penicillin G | Undetected | Undetected |
| Amoxicillin | Undetected | Undetected |
| Ampicillin | Undetected | Undetected |
| Cloxacillin | Undetected | Undetected |
| Benazocillin | Undetected | Undetected |
| Dicloxacillin | Undetected | Undetected |
| Cefuroxime | Undetected | Undetected |
| Cefquinoxime | Undetected | Undetected |
| Ceflonin | Undetected | Undetected |
| Cefazolin | Undetected | Undetected |
| Cefoperazone | Undetected | Undetected |
| Cefazolin | Undetected | Undetected |

Figure S1 TG and DTG curves of PR at heating rate of 10 °C/min

Figure S2 Effect of cycle time on the TC adsorption capacity of IKBCH

Figure S3 TC adsorption mechanism schematic diagram