Supporting Information file

FT-IR analysis

Concisely, to investigate tensile and bending vibrations in PVA/PEO/CS and PVA/PEO/CS/TG nanofibers, these samples were mixed with KBr (spectroscopy grade, Sigma Aldrich) powder and compressed into tablets. The resulting mixture was then inserted into the FT-IR sample holder and compacted. Spectra were captured within the scanning range of 200–4000 cm-1 using a spectral resolution of 4 cm-1 through the FT-IR spectrophotometer (IR Prestige-21 Shimadzu Spectrometer, Kyoto, Japan).

The FT-IR spectra of PEO, CS, PVA, and optimal nanofiber containing PVA/PEO/CS with TG extract are shown in Supplementary Figure 1.  In the case of PEO, the following stretching peaks were identified: C-C stretching vibrations (3386 cm−1), sp2 C‐H stretching vibrations (842.8 cm−1), C-O-C stretching frequency (1132.2 cm−1), C=C absorption band (1604.7 cm−1), C-O stretching frequency (1961.1 cm−1), C‐H stretching vibrations (2814.4 cm−1), CH2 weak stretching absorptions (2873.9 and 2927.2 cm−1), and finally O-H vibration (3414 cm−1). In addition, in the FT-IR spectrum of PEO, the bending vibrations of C-H (947.4 cm−1), C-O bending absorptions (1033.8, 1062.7, and 1109.6 cm−1), CH2 bending vibrations (1371.3 and 1427.3 cm−1), and eventually bending vibration of O-H (1591.2 cm-1) were characterized (Farea et al., 2020).

The main functional groups appearing in the IR spectrum of CS are as follows: bending vibrations of C-O at 993.3, 1026.13, and 1072.04 cm-1, stretching vibration of C-O-C at 1153.4 cm-1, bending vibration of C-N at 1217 cm-1, stretching vibration of C-H in 1421.5 cm-1, stretching vibrations of CH2-OH, CH-OH, and C-H in 1381, 1641.4, 2862.3 and 2916.4 cm-1, respectively. As the hydrogen bond is formed between the NH2 and the O-H groups in chitosan, the resulting stretching absorptions appear in the range of 3307.3 to 3464.1 cm-1 (Fernandes Queiroz et al., 2014).

In the FT-IR spectrum of PVA, the peak shown at 840.9 cm-1 was assigned to the symmetrical C-C stretching vibration. C-H bending vibration and C-O-C stretching vibration appeared at 947.4 and 1132.2 cm-1, respectively. Also, vibrations at 10333.8, 1062.7, and 1109 cm-1 were related to C-O bending vibrations. The peaks shown in 1371.3 and 1427.3 cm-1 were attributed to the bending vibrations of the CH2 group. The bending vibration and stretching vibration of O-H appeared in 1591.2 and 3332.9 cm-1, respectively. Besides, C=C and C=O stretching vibrations can also be seen in 1651.9 and 1732.0 cm-1, respectively (Uma Maheshwari et al., 2014).

Supplementary Figure 1. FT-IR spectra of polymers and polymer + extract, PEO, CS, and PVA.

References

Farea, M. O., Abdelghany, A. M., Meikhail, M. S., and Oraby, A. H. (2020). Effect of cesium bromide on the structural, optical, thermal and electrical properties of polyvinyl alcohol and polyethylene oxide. J. Mater. Res. Technol. 9, 1530–1538. doi: 10.1016/j.jmrt.2019.11.078

Fernandes Queiroz, M., Melo, K., Sabry, D., Sassaki, G., and Rocha, H. (2014). Does the Use of Chitosan Contribute to Oxalate Kidney Stone Formation? Mar. Drugs 13, 141–158. doi: 10.3390/md13010141

Uma Maheshwari, S., Samuel, V. K., and Nagiah, N. (2014). Fabrication and evaluation of (PVA/HAp/PCL) bilayer composites as potential scaffolds for bone tissue regeneration application. Ceram. Int. 40, 8469–8477. doi: 10.1016/j.ceramint.2014.01.058