Supplementary Materials

Table of Contents

Tables

- Table SM1. Multi-database validation between Scopus and Web of Science: AI, ML, and DL in Mg-alloys

- Table SM2 AZ31 and AZ31B alloys

- Table SM3 Al-Mg and Al-based alloys

- Table SM4 Advanced models (CNN, GBT, Graph-based)

- Table SM5 Cluster 2: Alloy composition and mechanical property optimization

- Table SM6 Cluster 2: corrosion, microstructure, and phase prediction

- Table SM7 Cluster 9: alloy composition and design strategies

- Table SM8 Cluster 3: atomic-scale simulations and ML potentials

- Table SM9 Cluster 6: first-principles and active learning approaches

- Table SM10 Cluster 4: AI in welding and advanced processing techniques

- Table SM11 Cluster 5: biomaterials and microstructural optimization

- Table SM12 Cluster 6: corrosion modeling

- Table SM13 Cluster 7: data-driven design and optimization techniques

- Table SM14. Actionable AI strategies and deployment challenges across key Mg alloy application dmains

Figures

- Figure SM1. CNN-based microstructure-to-strength prediction workflow

- Figure SM2.  ML-based prediction framework for heat treatment effects on mechanical properties in Mg alloys

- Figure SM3. SHAP summary plot for biodegradation rate prediction in Mg alloys

- Figure SM4. Time-series deep learning framework for grain growth prediction in Mg alloys

- Figure SM5. Data-driven optimization workflow for Mg alloy design

Table SM1. Multi-database validation between Scopus and Web of Science: AI, ML, and DL in Mg-alloys

| Validation Element | Database 1: Scopus | Database 2: Web of Science | Overlap | Similarity (%) |
| --- | --- | --- | --- | --- |
| Author Keywords (Top 20) | Machine Learning, Magnesium Alloys, Alloy Design, Magnesium Alloy, Mechanical Properties, Magnesium, Deep Learning, Corrosion, DFT, Mg Alloys, Molecular Dynamics, ANN, Aluminum Alloy, AI, Genetic Algorithm, Active Learning, Mg Alloy, Corrosion Behavior, DFT, Corrosion Resistance | Machine Learning, Magnesium Alloys, Magnesium, Magnesium Alloy, Mechanical Properties, Corrosion, DFT, Mg Alloys, Molecular Dynamics, ANN, Deep Learning, Aluminum Alloy, AI, Genetic Algorithm, Active Learning, Microstructure, Alloy Design, Friction Stir Welding, Prediction, Wear | 17 out of 20 | 85% |
| Index Keywords (Top 20) | Magnesium Alloys, Machine-Learning, Aluminum Alloys, Forecasting, Zinc Alloys, Binary Alloys, Copper Alloys, Learning Systems, Tensile Strength, Ternary Alloys, Mg Alloy, Machine Learning Models, Property, DFT, Neural Networks, Corrosion Resistance, Corrosive Effects, Deep Learning, Article, Density Functional Theory | Microstructure, Mechanical-Properties, Behavior, Magnesium, Magnesium Alloy, Strength, Ductility, Mg, Alloys, Evolution, Design, Prediction, Deformation, Temperature, Texture, Al, Aluminum, Corrosion, AI, DL | 16 out of 20 | 80% |
| Authors (Top 20) | Pan Fusheng, Tang Aitao, Zeng Xiaoqin, Lamaka Sviatlana V., Lee Taekyung, Wang Han, Wang Li, Würger Tim, Yu Jinyeong, Zheludkevich Mikhail L., Fu Huadong, Jiang Lei, Li Yuanyuan, Lu Guimin, Mi Xiaoxi, Mishra Akshansh, Wang Leyun, Xie Jianxin, Zhu Gaoming, Shaban Mahmoud | Pan Fusheng, Feiler Christian, Zheludkevich Mikhail L., Tang Aitao, Lamaka Sviatlana V., Wuerger Tim, Zeng Xiaoqin, Alsunaydih Fahad Nasser, Hoeche Daniel, Lee Taekyung, Meissner Robert H., Yu Jinyeong, Chen Ding, Vaghefinazari Bahram, Alawad Majed O., Wang Li, Mi Xiaoxi, Li Yuanyuan, Mishra Akshansh, Moses Atwakyire | 14 out of 20 | 70% |
| Sources (Top 20) | Materials Today Communications, Journal of Magnesium and Alloys, Computational Materials Science, Acta Materialia, Materials Letters, Journal of Materials Research and Technology, Journal of Alloys and Compounds, Materials and Design, Physical Review Materials, JOM, Journal of Materials Science and Technology, Materials, Materials Transactions, npj Computational Materials, Advanced Engineering Materials, Computers, Materials and Continua, Corrosion Science, npj Computational Materials, Journal of Applied Physics, Materials Characterization | Materials Today Communications, Journal of Magnesium and Alloys, Computational Materials Science, Journal of Materials Research and Technology-JMR&T, Journal of Materials Science & Technology, International Journal of Hydrogen Energy, Acta Materialia, Journal of Materials Science & Technology, Journal of Materials Informatics, Crystals, npj Materials Degradation, Applied Sciences-Basel, Corrosion Science, Advanced Engineering Materials, npj Computational Materials, Energy Storage Materials, International Journal of Interactive Design and Manufacturing, JOM, Scientific Reports, Mechanics of Materials | 16 out of 20 | 80% |
| Countries (Top 20) | China, USA, India, South Korea, Germany, Japan, United Kingdom, Australia, Switzerland, Canada, Saudi Arabia, Iran, Turkey, Russia, Spain, Taiwan, Egypt, Italy, Austria, Belgium | China, India, USA, Germany, South Korea, Australia, Saudi Arabia, Canada, Egypt, England, Iran, Russia, Taiwan, Turkey, France, Japan, Spain, Switzerland, Norway, Malaysia | 17 out of 20 | 85% |

Table SM2 Cluster 1: AZ31 and AZ31B alloys

| Ref. | Material/ Alloy | Target Property | ML/ANN Approach | Key Highlights/ Findings |
| --- | --- | --- | --- | --- |
| (Yu et al., 2024) | - AZ31 Mg alloy | - Low-cycle fatigue life | - Hybrid - ML/Energy-based model | - Outperformed traditional fatigue models - Accurate in multiple loading directions |
| (Wang et al., 2024a) |  | - Maximum thinning rate | - Hybrid BPNN-RF - with GA and DBO | - Best formability at 250Â°C - Resistance coefficient had the most substantial impact - 0.32% prediction error |
| (Zhang et al., 2023b) |  | - Tensile properties vs texture | - Artificial Neural Network | - ANN-linked texture features - (Imax, D, PLD, PTD) to yield strength and elongation |
| (Murugesan et al., 2023) | - AZ31B Mg alloy | - Flow stress | - BP-ANN - GABP-ANN - CFBP-ANN | - CFBP-ANN had the best prediction - Models trained on strain temp, and strain rate data |
| (Yadav and Khurana, 2022) |  | - Tensile strength - Elongation - Hardness - Grain size | - ANN + Genetic Algorithm | - Validated optimum joint performance (<3% error) - GA used for multi-objective optimization |
| (Jaafreh et al., 2022) | - Pure Mg and AZ31 | - Stress concentration (KAM) | - ERT, RF - MLP, LR - DT, KNN - NBC | - ERT best accuracy - Grain size was most important - SC lower in fine-grain sizes |

Table SM3 Cluster 1: Al-Mg and Al-based alloys

| Ref. | Material/ Alloy | Target Property | ML/ANN Approach | Key Highlights/ Findings |
| --- | --- | --- | --- | --- |
| (Jain et al., 2024) | - Al-Mg-X alloys | - Hardness | - CatBoost - Ensemble ML models | - CatBoost showed superior hardness prediction - Compiled composition - Aging, and property data |
| (Chandana and Kamesh, 2024) | - Mg-based alloys | - Hydrogen storage/ release capacity | - ANN with Bayesian | - R² of 0.86 to 0.93 - Key factors included particle size Mg content and pressure |
| (Yu et al., 2024) | - AZ31 Mg alloy | - Low-cycle fatigue life | - Hybrid ML/ Energy-based model | - Outperformed traditional fatigue models - Accurate in multiple loading directions |
| (El-Garaihy et al., 2024) | - ZX30 Mg alloy | - Grain size - Corrosion rate - Yield strength | - ANN - Gaussian Process Regression - Simulated Annealing | - Route Bc and pass number crucial - Strong correlation with yield strength and corrosion resistance |
| (Zhu et al., 2025b) | - Cu-Cr-Zr-Mg-Ti alloy | - Tensile strength - Electrical conductivity | - BP neural network - GA | - 668 MPa tensile strength achieved - Micro-alloying effects captured via ANN. |
| (Bai et al., 2024) | - Al-Zn-Mg-Cu-Zr alloy | - Flow stress - Dislocation density | - BP-ANN - Correlation K-means clustering | - R² = 98.67% for stress - Linked energy dissipation with microstructure (DRX, grain boundaries) |
| (Efa, 2024) | - AA7075 - AZ61A with Ti-interlayer | - Residual stress - Equivalent strain - Peak temperature | - BP neural network with gradient descent | - Ti-interlayer reduced residual stress - ANN predicted optimal process settings accurately |
| (Gurugubelli et al., 2023) | - Al-Mg alloys - (5000 series) | - Tensile strength | - AI with Python - Ansys simulations | - Simulated tensile test equivalent to experiments - AI as an alternative to lab testing |
| (Li et al., 2024d) | - Mg-2Ho alloy | - Flow stress | - PSO-BP ANN | - PSO-BP ANN outperformed the Arrhenius model (R² = 0.99948) - Captured DRX mechanisms |
| (Xue et al., 2023) | - Al-Mg alloy | - Corrosion resistance (NAMLT) | - ML framework (unspecified) | - Predicted corrosion resistance from limited data - Mg% - Annealing temp/time critical |
| (Mishra, 2024a) | - Mg alloys - FSW | - Ultimate tensile strength | - Decision Trees - XGBoost, ANN - RF - Gradient Boosting - AdaBoost | - XGBoost had the highest R² = 0.81 - Mg alloy type was the most important feature |
| (Jiang et al., 2024a) | - Advanced - Al-Zn-Mg-Cu-Ti -Cr-Zr alloy | - UTS - Toughness - Corrosion resistance | - Interpretable ML | - Ti, Cr, Zr enhanced all properties - Explained elemental impact using ML. |
| (Troncoso et al., 2023) | - Mg-10%Al alloy | - Twinning interface recognition | - Advanced ML | - Used stress fields to identify interfaces - Prismatic interfaces drive twin growth |
| (Wang et al., 2023a) | - Al-Li alloys | - Tensile strength - Yield strength | - RBF and BP neural networks | - RBF outperformed BP - Validated with experiments - Improved efficiency |
| (Byun et al., 2024) | - ZK60 Mg alloy | - Anisotropic deformation behavior | - GAN-aided GRU model | - Excellent generalization in flow prediction - Effective with small datasets and multiple directions |
| (Medghalchi et al., 2023) | - Mg-4.65Al-2.82Ca alloy | - Damage mechanism (microcracks, decohesion) | - YOLOv5 DL (object detection) | - Damage mechanisms vary with strain rate - DL detected crack evolution and orientation changes |
| (Pei et al., 2024b) | - Mg-Gd-Y-Zr alloy | - Stress-strain behavior (hot-forming) | - ANN - ISV model - Arrhenius | - ANN best fits the original data - ISV model is effective - under complex loading and embedded in ABAQUS. |
| (Li et al., 2023) | - 7075 Al alloy | - Slurry temp - Uniformity (ECP process) | - GA-BPNN | - R² = 0.9988 for average temp - Excellent fit for temp prediction |
| (Mokhtari et al., 2024) | - Al-Mg alloys | - Tensile strength - Stiffness | - ANN, GRU - LSTM, RNN (DNNs) | - RNN and LSTM outperformed other models - DNNs with memory were best for predicting tensile properties |
| (Sun and Liu, 2023) | - Mg alloys | - Uncertainty quantification (performance) | - Deep Neural Network classifier + SGD | - Used DNN to - optimize performance bounds - Helped in safety design for Mg alloys |
| (Shaban et al., 2023) | - ZK30 Mg alloy | - Grain size - Hardness - Corrosion | - Linear regression - Gaussian process - SVR | - Route Bc with four passes optimal - The model showed that the die angle had little effect on grain refinement. |
| (Jagadeesh and Setti, 2023) | - Mg Ze41A alloy | - Wear rate - Tribological behavior | - ANN | - Wear maps built - Predicted wear characteristics with a 3.4% error. |
| (Ma et al., 2022) | - Cast Al - Mg-based alloys | - Grain size | - Various ML methods (review) | - ML was highlighted as effective for data-driven grain size prediction across compositions and conditions |

Table SM4 Cluster 1: Advanced models (CNN, GBT, Graph-based)

| Ref. | Material/Alloy | Target Property | ML/ANN Approach | Key Highlights/ Findings |
| --- | --- | --- | --- | --- |
| (Kim et al., 2024) | - Al-Ti-Cr - Al-/Mg-based alloys | - Specific hardness | - Ensemble ML (ANN, CNN, RF, etc.) | - New high-hardness alloys - Explainable AI to interpret results |
| (Lopes Marinho et al., 2024) | - Mg-based biodegradable implants | - Degradation - Osseointegration (image segmentation) | - CNNs (U-Net, HR-Net, nnU-Net) | - 2D nnU-Net had the best segmentation performance on images - Degradation layer most challenging to predict |
| (Nithin et al., 2022) | - Al-Si-Mg alloy | - Grain prediction (a-Al grains) | - CNN | - CNN predicted a-Al grains with >90% accuracy - Extrusion ratio = 2 showed the best properties |
| (Masood Chaudry et al., 2021) | - Al-Cu-Mg-x - alloys | - Hardness | - Gradient Boosted Trees (GBT) | - GBT predicted the hardness of the unexplored Al alloys effectively using literature data |
| (Shu et al., 2022) | - Polycrystalline Mg alloys | - Microstructure- property prediction | - HGGAT (graph attention network) | - HGGAT outperformed ML baselines - Proposed grain knowledge graph for performance prediction. |

Table SM5 Cluster 2: Alloy composition and mechanical property optimization

| Ref. | AI/ML Technique Used | Target Material/ System | Predicted Property/ Output | Key Findings |
| --- | --- | --- | --- | --- |
| (Wang et al., 2025) | - Interpretable ML (Data Augmentation + Reconstruction) | - Low-alloyed Mg Alloys | - Ultimate tensile strength - Elongation-to-failure | - High accuracy (R² > 95%) - New Mg alloy (MZAX2000) shows excellent strength-ductility |
| (Li et al., 2024a) | - DL Potential | - Al2CuMg Phases in Al-Cu-Mg Alloy | - Crystal structure - Mechanical/thermal properties | - Highest rigidity and tensile strength - Highest thermal - conductivity |
| (Yang et al., 2024) | - RF Regression (RFReg) | - SiCp/Al Composites with Cu | - Mechanical properties (tensile strength) | - ML-designed composite achieved 561 MPa after processing |
| (Mo et al., 2025) | - Active Learning with Bagging | - Al-Mg-Zn Alloys | - Strength-ductility balance - (UTS and EL) | - New alloy - 602 MPa UTS and 15.1% EL - Validated via Microstructural analysis |
| (Anne et al., 2024) | - Decision Tree - Multi-Layer Perceptron (MLP) | - Mg/Al-Ce Hybrid Composite | - Structure-property relationships | - Strength and hardness improved 2.36x - ML captures deformation-property trends |
| (Mi et al., 2024) | - Regression-based Bayesian Optimization Active Learning Model (RBOALM) | - Mg-Mn-based Wrought Alloys | - Mechanical properties (UTS, YS, EL) | - New alloys - High strength - Elongation revealed |
| (Peng et al., 2023) | - Active Learning - Revised LAsou Method | - Mg3Bi2-xSbx Alloy | - Atomic configurations | - 90-atom unit cells yield realistic structures - XRD matches experiment |
| (Juan et al., 2024) | - ML-based Property Optimization | - Al-Zn-Mg-Cu Alloys | - Strength and toughness | - Trace Hf addition improves strength - Alloy validated with superior properties |
| (Jiang et al., 2021) | - Deep Potential - DP-GEN | - Al-Cu-Mg Alloy System | - Potential Energy Surface (PES) | - Model consistent with first-principles - Suitable for full-range atomistic modeling |

Table SM6 Cluster 2: Corrosion, microstructure, and phase prediction

| Ref. | AI/ML Technique Used | Target Material/ System | Predicted Property/ Output | Methodology/ Model Details | Key Findings |
| --- | --- | --- | --- | --- | --- |
| (Kuriki et al., 2024) | - Multimodal Deep Learning (MDL) | - As-cast Mg/ LPSO two- phase alloys | - 3D local strain distribution | - 3D microstructure descriptors + DL - Occlusion sensitivity - Correlation analysis for - feature importance | - High strain occurs where the hard LPSO phase is elongated - Multimodal DL - improves prediction accuracy |
| (Liu et al., 2025b) | - MDL | - Thermal Barrier Coatings (TBCs) - Turbine blades | - TBC failure/ - lifetime prediction | - DL network modeling corrosion effects with microscale stress and damage models | - DL model accurately predicts TBC spalling Lifetime within 20% of observed data |
| (Chen et al., 2024b) | - GA | - AZ61 Mg Alloy | - Rheological behavior - DRX grain growth | - GA-optimized Arrhenius Model + 3D Cellular Automata for microstructure evolution | - GA-Arrhenius accurately predicts material behavior - CA simulates DRX morphology |
| (Dai et al., 2024) | - ML | - WE43 Mg Alloy | - Corrosion behavior under protein adsorption and shear stress | - ML model to explore intrinsic corrosion mechanism under BSA and WSS | - BSA and WSS competitively accelerate corrosion - ML models - intrinsic mechanisms |
| (Chen et al., 2024a) | - ML | - Biodegradable Zn Alloys | - UTS - Corrosion rate | - ML models for UTS - CR with real-time visualization interface | - UTS prediction error 0.95% - CR 5.5% - Enables efficient Z - n-Mn alloy design |
| (Qi et al., 2025) | - Spatiotemporal DL (PredRNN, ConvLSTM) | - MAO-coated Mg Alloys | - Corrosion progression | - FEM-generated dataset - DL models trained to predict corrosion evolution | - PredRNN model outperforms in stability detail for long-term prediction |
| (Davydzenka et al., 2022) | - ML + Stochastic Augmentation | - Mg-based Alloy | - Image - segmentation accuracy | - Stochastic data - augmentation improved model training with limited data | - Segmentation accuracy improved from 81.1% to 90% with augmented data |
| (Li et al., 2025) | - Wasserstein Autoencoder + Property Predictor | - Fe-based Metallic Glasses | - Saturation magnetic flux density (Bs) | - Joint-WAE model for inverse design high-dimensional optimization | - Predicted unreported Fe-based MGs with Bs > 1.5 T validated experimentally |

Table SM7 Cluster 2: Alloy composition and design strategies

| Ref. | Alloy System / Base Alloy | Design Strategy/ Method Used | Target Properties | Key Alloying Elements | Main Findings/ Outcome |
| --- | --- | --- | --- | --- | --- |
| (Zhang et al., 2025c) | - Al-Zn-Mg-Cu (7075) | - Kriging-assisted Two Archive algorithm (KTA2) | - Strength - Plasticity - Grain refinement | - Ca - Y | - Improved joint properties in 4 iterations - Reduced grain size and eliminated columnar grains |
| (Zhang et al., 2024a) | - Cu-Ni-Co-Si-Mg | - SHAP analysis + physicochemical screening | - Strength - Conductivity - Sustainability | - Cr (substitution for Co) | - 64% Co reduction - Retained high UTS and conductivity |
| (Feng et al., 2023) | - Al-Mg-Si | - NSGA-II GA | - Strength - Corrosion resistance | - Mn - Cr - Fe - Zr - Ti | - Improved YS/UTS - Corrosion resistance with low Cu/Mg/Si |
| (Zhang et al., 2023a) | - Al-Si-Mg-Sr-Ti | - Bayesian optimization + thermodynamics | - Strength - Ductility | - Sr - Ti | - Designed Ti-modified alloy - Validated Composition -property relation |
| (Cheng et al., 2024) | - Mg-Al | - Generative model + automatic differentiation | - Structure prediction | - Mg - Al | - Predicted five stable Mg-Al structures with application potential |
| (Jiang et al., 2022) | - Al-Mg-Zn (Cu, Cr, Mn, Ti, Zr) | - Property-oriented MLDS | - UTS - Ductility - Toughness | - Mg - Zn - Cr - Mn - Ti - Zr | - Discovered novel alloys with UTS up to 736 MPa |
| (Yanase et al., 2022) | - Al-Si-Mg | - SLM + ML analysis | - Relative density - Microstructure | - Si - Mg | - Double scanning improved density - ML identified key parameters |
| (Liu et al., 2020) | - AlSi10Mg | - GPR | - Density - Strength - Ductility | - Si - Mg | - Optimized LPBF window - Improved Mechanical properties |

Table SM8 Cluster 3: Atomic-scale simulations and ML potentials

| Ref. | Material/ System Studied | Simulation Method(s) | ML Technique/ Model | Key Focus/ Target Property | Key Findings/ Outcomes |
| --- | --- | --- | --- | --- | --- |
| (Jiang et al., 2024b) | - NLi4-BGra/ MgH2 Heterojunction | - DFT - MD | - DFT + ML for material prediction | - Hydrogen storage - Desorption temperature | - ML-assisted DFT predicted improved Mg-alloy hydrides - Modulation of H-desorption via heterojunction substitution validated |
| (Geng et al., 2025) | - MgCu alloys (monocrystal/ polycrystalline) | - DFT - MD | - ML Force Field (MLFF) | - Strength- concentration relation - Yield strength | - MLFF enables accurate mechanical property prediction at low Cu concentrations - Refined strength understanding |
| (Deng, 2024) | - Mg-Fe-O system | - Large-scale simulations with ML potential | - DL Interatomic - Potential | - MgO exsolution processes - Geodynamo energy source | - Unified DL potential predicts MgO exsolution phase and rate - Refining geodynamic models |
| (Fang et al., 2025) | - 1155 binary alloy catalysts for glucose hydrogenation | - DFT - Microkinetic simulation | - Light Gradient Boosting Machine (LGBM) | - Adsorption energies - Catalytic activity | - LGBM accurately predicts adsorption energies - Identified 9 high-activity catalysts |
| (Zhang et al., 2025b) | - BCC Mg-Li-Al alloys (single crystal and polycrystalline) | - DFT - ML-based atomistic simulations | - ML Potential Energy Surface | - Plastic deformation - Phase transition - Twin strengthening | - Revealed BCC-FCC-BCC-HCP phase transition in single crystal Mg-Li-Al - Twin strengthening absent in polycrystalline |
| (Chen et al., 2025) | - Dual-site M-COFs MgFe-S-COF MgZn-S-COF | - DFT | - ML screening of 136 candidates | - CO2 reduction to C2 products - Charge distribution | - DFT & ML identified catalysts |
| (Menon et al., 2024) | - Micro-scale Polycrystalline Mg-Y alloys | - MS - MD - DFT | - Surrogate model with stacking cross- validation | - Grain boundary segregation thermodynamics | - Predicted Y segregation free energies with uncertainty - Model agrees with experimental results |
| (Feng and Lu, 2024) | - Hydrated MgCl2-NaCl-KCl (MNK) molten salt | - AIMD - DPMD | - Deep Potential (DP) - DP-GEN | - Thermophysical properties - Diffusion - Viscosity - Conductivity | - Efficient ML potential development - Accurately predicts temperature-dependent properties of MNK s ystem |
| (Wang et al., 2024b) | - Binary Mg intermetallics | - DFT - HER kinetics model | - Regression model using Wf and WFIE | - Corrosion resistance - Hydrogen adsorption energy | - ML predicts corrosion-resistant intermetallics - Model validated with low RMSE on new alloys |
| (Motamedi et al., 2023) | - Al-Mg-Zn alloy | - MD simulation | - GLM - ANN - DT - RF | - Tensile properties under different conditions | - ANN best for predictions - Parameter tuning improved DT and RF accuracy |
| (Wang et al., 2021) | - Ternary Mg alloys (RE-free) | - DFT | - Non-linear regression model | - Stacking fault energy - Ductility | - ML predicted low SFE alloys validated by DFT - RE-free ductile alloys |
| (Tian and Yu, 2021) | - Mg-Cd binary alloy | - DFT - Cluster Expansion - Monte Carlo | - Semi-automated phase detection algorithm | - Phase diagram prediction - Transition behavior | - First quantification of uncertainty in DFT-based phase diagrams - Detected configurational disorder |
| (Álvarez-Zapatero et al., 2021) | - ZnMg nanoalloys | - DFT - Basin-hopping | - Neural Network (NN) potential | - Energy landscape - Stability | - NN predicts stable structures accurately - Structural/electronic traits of nanoalloys |
| (Xue et al., 2022) | - Al-Mg-Zn-Er-Zr alloys | - EBSD - Experimental validation | - ANN vs. Arrhenius model | - Hot deformation behavior | - ANN outperforms traditional models - Accurately predicts deformation and dislocation trends |
| (Messina et al., 2021) | - Mg-Al alloys (grain boundaries) | - Atomistic simulations | - ML for segregation energetics | - Grain boundary segregation - Corrosion resistance | - Al segregation varies with GB structure - ML quantifies energetics for better alloy design |

Table SM9 Cluster 3: First-principles and active learning approaches

| Ref. | Materials/ System Studied | ML/ Computational Approach | Key Features/ Variables | Main Findings |
| --- | --- | --- | --- | --- |
| (Zhu et al., 2025a) | - Comprehensive database of various Mg alloys | - GBR - A-SMOTE algorithm | - 28 features - Key ones: ultimate tensile strength, yield strength, Ce, La | - GBR: 89% accuracy - Inverse design of Mg alloys with optimal properties |
| (Ling et al., 2024) | - Binary Mg alloys (e.g., Mg-Ca, Mg-Zn, Mg-Al) | - XGB | - Cell voltage - Utilization efficiency - Specific capacity - Specific energy | - Identified Mg-Ca as best anode - Good agreement between predicted and experimental results |
| (Zhang et al., 2025a) | - Mg-Ca-Zn alloys with different aging treatments | - RF - AL | - Alloy composition - Aging time and temperature | - Peak hardness: 71.10 Hv predicted and validated - RF outperformed other models |
| (Liang et al., 2024) | - 29 Mg-based binary alloys | - First-principles (DFT) + ML analysis | - Valence difference - Electron configuration - Solubility - Electronegativity | - Alloys with s/p-block elements showed higher conductivity |
| (Jain et al., 2025a) | - Mg-based rare earth alloys with different thermomechanical treatments | - KNN - Performance evaluation (R², MAE, RMSE) | - Ultimate tensile strength - Yield strength - Elongation. | - KNN: R² = 0.955 - Effective in predicting mechanical behavior |
| (Ghorbani et al., 2024) | - Various Mg alloys | - GPR - AL - Bayesian optimization | - Prediction and uncertainty balance via upper confidence bound acquisition function | - Overcame prediction error dependency - Validated strategy via regret analysis - Web tool developed |
| (Zhang et al., 2024c) | - 38 binary Mg solid solutions | - First-principles + ML feature screening | - DOS variance - Valence difference - Electronic structure descriptors | - Phonon contribution <10% - Key descriptors identified for thermal conductivity |
| (Wu et al., 2025b) | - Electrolyte additives for Mg-0.2Ca anodes | - ML-based adaptive design | - Additive properties impacting voltage - Efficiency - Specific energy | - Discovered 2,3-dihydroxynaphthalene with highest specific energy (3.37 kWh/kg) |
| (Mo et al., 2025) | - Al-5.27Mg-2.8Zn based multi-element alloy | - Bagging + AL - Pareto front optimization | - UTS - EL - Alloy composition | - Designed alloy achieved 602 MPa UTS and 15.1% EL - Microstructure analysis confirmed findings |
| (Menon et al., 2024) | - Y in polycrystalline Mg (symmetric tilt grain boundaries) | - Spectral model - Stacking CV regressors with physics-informed features | - Per-site segregation energy/ free energy spectra | - Predicted Y segregation tendencies aligned with experiments |
| (Ji et al., 2024) | - Al-Sc-Cu based alloys | - Reinforcement self-learning ML - Work function prediction | - Stress-strain - Corrosion resistance - H-trapping | - Elongation reached ~30% - Verified experimentally |
| (He et al., 2023) | - Mg alloy dataset from high-throughput DFT | - KRR - DeePMD - (DL) | - Atomic descriptors - Formation energy | - DeePMD is more accurate - KRR more efficient - RMSE down to 0.43 meV/atom |
| (Wang et al., 2023c) | - Binary Mg intermetallics | - Active learning - DFT - Voronoi-based H adsorption modeling | - H adsorption energy - Electron transfer - Surface stability | - Identified intermetallics that suppress HER - MAE = 0.196 eV with <1% dataset |
| (Chen et al., 2022a) | - Various solutes in Mg matrix | - RF - Decision Tree | - Formation energy - Electronegativity - Work function - Atomic radius | - Identified 4 key features for solubility classification |
| (Wang et al., 2021) | - 300 ternary RE-free Mg alloy systems | - ML regression on DFT SFE data | - Volume - Oonization energy - Bulk modulus | - Predicted novel ductile alloys - Validated by DFT and experiments |
| (Chen et al., 2022b) | - 24 binary and 88 ternary Mg alloys | - ML on DFT derived features | - Atomic substitution - Volume diff. c/a ratio, formation energy | - Strong correlations between interaction features and elemental properties |
| (Choudhuri, 2021) | - Precipitate in Mg matrix | - DFT-based modeling of precipitate/ matrix structure | - Phonon DOS - Covalent bonding - Template-nucleus stability | - Nucleation starts with substructures stabilized in Mg |
| (Chen et al., 2020) | - ZE62 Mg alloy (Mg-Zn-RE) | - Iterative multi-objective ML optimization | - Aging treatment parameters | - 27% strength - 13.5% ductility improvement in 4 experiments |
| (Jaafreh et al., 2023) | - MgBe13 - MgPd2 and related IMCs | - ML with moduli-based proxies + DFT validation | - G/B ratio - Charge density - ELF | - DB behavior predictions aligned with DFT - Guides IMC screening |
| (Batalović et al., 2022) | - Mg-Ni-M intermetallics | - MEGNet - Transfer learning | - Crystal structure - Formation enthalpy | - Fast accurate prediction of hydride enthalpy for hydrogen storage |
| (Pei and Yin, 2019) | - Various solutes in Mg matrix | - Gaussian Process Classification | - Solute properties - Ductility mechanism proxies | - Clarified competing ductility mechanisms via solute screening |

Table SM10 Cluster 4: AI in welding and advanced processing techniques

| Ref. | Focus Area | Material/ System Studied | AI/ML Technique Used | Application/ Outcome | Key Findings |
| --- | --- | --- | --- | --- | --- |
| (Jiang et al., 2024b) | - Hydrogen Storage Materials | - NLi4-BGra/MgH2 heterojunctions - Mg1-XMeXH2 | - ML with DFT and MD | - Tuning hydrogen - desorption temperature | - ML-guided substitution modulates hydrogen-desorption temperature - Validated via MD and electronic structure analysis |
| (B et al., 2025) | - FSW | - AZ31B Mg Alloy Yttrium Oxide | - DNN - 1D-CNN - Gaussian Process Regression | - Prediction of Mechanical properties | - FSP improves hardness - Wear and corrosion resistance - ML models predict performance effectively |
| (Athul et al., 2025) | - Hydrogen Storage Prediction | - Intermetallic Hydrides (Mg, Li, Ge based) | - RF | - Prediction of hydrogen storage capacity and properties | - Identified stable compounds with high HSC - ML reduces discovery time using elemental attributes. |
| (Österreicher et al., 2024) | - Thermo- mechanical Processing | - Al-Mg-Si Alloys | - Feedforward Neural Network | - Prediction of grain structures during extrusion | - In-situ conductometry + ML enables prediction of extrudate structure |
| (Mishra, 2024a) | - FSW | - Mg Alloys - (AM20, AZ61A, AZ31B, AZ31) | - Decision Trees - XGBoost - ANN - RF - Gradient Boosting - AdaBoost | - Prediction of - Ultimate Tensile Strength | - XGBoost achieved highest R² (0.81) - Alloy type most significant feature |
| (Menze et al., 2024) | - Biodegradable - Mg Implants | - Resoloy Mg scaffolds in coronary arteries | - U-Net (Convolutional Neural Network) | - Segmentation of images for degradation analysis | - DL-aided image analysis reveals slower degradation with thinner struts and paclitaxel - Correlated with lumen loss and recoil |
| (Bahari-Sambran et al., 2024) | - Superplastic Deformation Analysis | - ZK30 Mg Alloy | - RF - ANN | - Prediction of high temperature flow stress | - ANN accurately predicts flow stress - Grain size affects superplastic behavior significantly |
| (Maqbool et al., 2024) | - Corrosion Rate Prediction | - WE43 Mg Alloy | - ML with PSO generated synthetic data - SHAP analysis | - Corrosion rate prediction based on FSP parameters | - Shoulder diameter most significant - GUI developed - Improved prediction using virtual data. |
| (Mishra, 2024b) | - Text Summarization in Welding Research | - FSW Mg Alloy Abstracts | - Text Rank - Lex Rank - LSA - Luhn - KL-SUM - ROUGE | - Performance comparison of NLP summarization methods | - Luhn performed best based on F1 score - NLP useful for structuring welding literature |
| (Wiese et al., 2023) | - Material Design Optimization | - Mg-Gd Alloys | - Shallow ANN - Hyperparameter Optimization | - Prediction of mechanical properties from alloy content and process | - Accurate predictions of anisotropic behavior - ML model better than - linear regression. |
| (Díaz-Romero et al., 2023) | - Al Scrap Sorting | - Post-consumer Al Scrap | - UNet - DenseNet - DL Fusion | - Scrap classification by alloy type | - Fusion model achieves high accuracy (F1 up to 99%) - Enables efficient alloy-based sorting |
| (Rahnama and Sridhar, 2019) | - Hydride Clustering Analysis | - DOE Hydride Database | - K-means Clustering - Kernel Density - Estimation | - Cluster analysis for hydrogen storage materials | - 3 optimal clusters identified - Mg-based complex hydrides and A2B group together parameter removal impacts clustering |

Table SM11 Cluster 5: Biomaterials and microstructural optimization

| Ref. | Focus Area/ Alloy System | ML/DL Method | Key Findings/Application Area | Application Area |
| --- | --- | --- | --- | --- |
| (Huang et al., 2024) | - Effect of ECAP and reinforcement on properties - AZ61 Mg + composites | - ML | - ECAP and reinforcement improved hardness - YS, and modulus - Microstructure-phase homogeneity positively correlated with strength | - Structural materials |
| (Chen et al., 2020) | - Multi-objective optimization of aging treatment - ZE62 Mg alloy | - ML-assisted - Experiment Planning | - Optimized strength - (+27%) - Ductility (+13.5%) with just 4 experiments - Method accelerated design of aging parameters | - Alloy design methodology |
| (Li et al., 2021) | - SPD and implant mechanical behavior prediction - UFG biodegradable Mg alloys | - ANFIS - SVM - GEP - GP | - ANFIS and SVM accurately predicted fracture and implant behavior - SPD parameters critical for implant design | - Orthopedic implants |
| (Suh et al., 2022) | - Aging and precipitation property prediction - AZ61, AZ91 | - ANN + Decision Tree | - Mg17Al12 precipitation behavior - Yield strength predicted with >98% accuracy - SEM-only data extended dataset by 9x | - Aged structural alloys |
| (Zhang et al., 2020) | - SPD effect on implant alloy performance - ZK60 Mg (biodegradable) | - GEP - GP | - SPD via PTCAP improved mechanical performance - ML predicted optimal pass numbers and property trends | - Bone implants |
| (Yanase et al., 2022) | - SLM densification analysis - Al-10Si-0.35Mg | - ML | - ML identified scan pitch and speed as dominant parameters for densification - Double scan improved relative density >95% | - Additive manufacturing |
| (Liu et al., 2020) | - LPBF process window optimization - AlSi10Mg | - Gaussian Process Regression | - Optimized LPBF parameters for 99%+ density - Subtle cell morphology differences explained property variation | - Additive manufacturing |
| (Ma et al., 2025) | - Corrosion behavior of coated Mg alloys - PEO-coated WE43 Mg alloy | - CNN | - CNN predicted corrosion curve/ interface with ~1% error - Coating microstructure critical to corrosion resistance | - Biomedical implants |
| (Jain et al., 2025a) | - Property prediction under thermo-mechanical processing - Mg-RE alloys | - KNN | - KNN (R² = 0.955) - UTS - YS - Elongation predicted under various treatments | - Lightweight materials |
| (Wu et al., 2025a) | - Microstructure evolution with RE addition - A356 + Y aluminum alloy | - AIMD + DPMD Simulations | - Y refined microstructure - Removed MgSi - Reduced defects - Improved mechanical properties by up to 19.02% | - Automotive/ Aerospace |
| (Otieno et al., 2024) | - Phase and property prediction - Mg-Al-Cu-Mn-Zn alloys | - ANN - KNN - LDA - RF | - ANN: 98.7% accuracy - Predicted strengthening phases (e.g., Mg17Al12) - Verified by SEM/EDS and MatCalc | - Vehicle/ Aerospace |
| (Geng et al., 2025) | - Strength prediction at low Cu content - Mg-Cu solid solutions | - MLFF | - MLFF accurately predicted strength trends - Ductility and YS improved <0.43 at% Cu - Grain refinement the effect was minor | - Orthopedic biomaterials |
| (Farooq et al., 2025) | - Combustion behavior and ignition resistance - AZ31 - AZ91 - WE43 - Mg-Gd-Y-Zn-Zr | - Supervised/ Unsupervised ML | - Image processing + ML revealed ignition phases and morphologies - REEs formed protective oxides - Key for fire-resilient alloys | - Aerospace/ industrial |
| (Jain et al., 2025b) | - Generalized mechanical property prediction | - ET - RF - XGB | - Extra Trees gave best performance (R² = 97.2% for YS) - ML models accelerated alloy design with minimal intervention | - Tailored applications |
| (Raguraman et al., 2024) | - Microstructure- property-degradation relation - Multicomponent - Mg alloys - ZX10 (Mg-Zn-Ca-Mn) - alloy | - LASSO + Pearson correlation | - Grain size and Ca₂Mg₆Zn₃ phase dominated strength and corrosion - Highlights thermal processing role in biodegradable implant performance | - Orthopedic implant |
| (Zhu et al., 2025a) | - Mechanical property prediction - Mg alloys | - GBR | - GBR: 89% accuracy - Key features: UTS, YS, Ce, La - Inverse design using A-SMOTE - Low prediction error (0.5–9.6%) | - Structural materials |

Table SM12 Cluster 6: Corrosion modeling

| Ref. | Material/ Corrosion Context | AI/ML Method Used | Key Inputs/ Target Outputs | Model Performance | Highlights/ Applications |
| --- | --- | --- | --- | --- | --- |
| (Ma et al., 2025) | - PEO-coated WE43 Mg Alloy - Pitting corrosion under mechano-chemical loading | - CNN - Encoder - Decoder | - Coating microstructure (phase field data) - Corrosion curve - Interface evolution | - Avg. error ~1% - Multi-input CNN superior | - Fast evaluation of biodegradable coatings |
| (Liu et al., 2025a) | - Mg Fracturing Balls - Corrosion - Strength balance | - Multi-objective - ML + Genetic Algorithm | - Element ratios from corrosion - Strength DB - Corrosion rate - Compressive strength | - Accuracy: 0.93 on test set | - Discovered new Mg alloy with optimal properties |
| (Dargusch et al., 2024) | - Biodegradable WE43 Mg Alloy - In vivo corrosion - Hydrogen evolution | - ML-based image analysis + Atom Probe Tomography | - CT scan images - Nanophase data - In vivo hydrogen evolution - Corrosion rate | - Latent gas evolution found despite decreasing corrosion rate | - Revealed passivation mechanisms - Corrosion trends |
| (Chen et al., 2024a) | - Zn-Mn Based Biodegradable Alloy - Corrosion rate Strength prediction | - ML Models with real-time visualization interface | - Alloy composition - Mechanical test data - UTS - Corrosion Rate | - UTS error: 0.95% - CR error: 5.5% | - Dual-model strategy for alloy design |
| (Pei et al., 2024a) | - Mg-RE-Ni Alloys - Corrosion mechanism modeling | - ML | - Microstructure parameters of LPSO phase - Corrosion behavior | - Prediction accuracy > 93% | - Quantified Composition -structure-corrosion relationship |
| (Gu et al., 2024) | - AZ80 Mg Alloy - High-temp mechanical - prediction | - TCMSSA-ELM (Improved ELM) | - Temp, strain rate - Strain - Stress under hot deformation | - MAPE: 85.4% - R²: 0.99956 | - Optimized ML model for forming stage prediction |
| (Qi et al., 2025) | - MAO-coated Mg Alloys - Electrochemical corrosion behavior | - FEM + Spatiotemporal DL (PredRNN, ConvLSTM) | - Simulated corrosion data from FEM - Corrosion evolution (spatiotemporal) | - PredRNN outperformed ConvLSTM in stability/detail | - Accurate long-term corrosion forecasting tool |
| (Jiang et al., 2024a) | - Advanced Al Alloy - Stress corrosion - Strength Toughness | - Interpretable ML design strategy | - Intrinsic atomic/ - electronic factors - UTS - KIC - ISSRT | - Designed alloy met multiple property targets | - Selected Ti, Cr, Zr for improved corrosion resistance |
| (Gao et al., 2024) | - ZM6 Mg Alloy - Fatigue life under - internal defects | - XGBoost + Damage Mechanics Model | - Stress - Stress ratio - Defect coeff. - High cycle fatigue life | - High prediction accuracy - Tested with real defects | - Linked defect geometry with corrosion-fatigue |
| (Mondal et al., 2024) | - Mg Alloys for Implants - Review on ML-based corrosion modeling | - Multiscale ML models - ANN - RFR - LASSO, etc. | - Model structures - Alloy data - Implant physiology - Corrosion behavior prediction | - RFR best performer - LASSO/ANN less effective | - Comprehensive critical review for implant alloys |
| (Feng et al., 2024) | - Medical Mg Alloys (Anticorrosion Coatings) - Electroactive anticorrosion protection | - Thermodynamic Equilibrium Calculations | - TA/pH ratio - Chemical composition - Corrosion resistance improvement | - Validated by empirical corrosion trends | - New TA/pH-based coating design framework |
| (Feng et al., 2023) | - Al-Mg-Si Alloys - Strength vs. corrosion trade-off | - NSGA-II (Genetic ML Algorithm) | - Alloying elements (Cu, Mg, Si, etc.) - UTS - YS - Elongation - Corrosion resistance | - Developed 3 high-performance alloys | - Simultaneous strength - Corrosion optimization |
| (Li et al., 2024c) | - Light High-Entropy Alloys (LHEAs) - Phase prediction | - Gradient Boosting Classifier | - Elemental features - Solid solution phase type | - Accuracy: 91.7% - F1: 89.2% | - LHEA prediction framework validated |
| (Pagadala et al., 2023) | - Mg-Sn Alloy - (Implants) - Corrosion rate | - XGBoost | - EIS and Tafel data - Corrosion rate prediction | - R2: 0.961 (EIS), 0.6145 (Tafel) | - Accurate prediction in bio-environment |
| (Ghorbani et al., 2023) | - Mg Alloys (General) - Composition -property modeling | - RF - NN - Cross-validation | - Atomic & thermo features - UTS, ductility | - RF: 80% - NN: 70% accuracy | - Created GUI for property prediction |
| (Suh et al., 2023) | - ZMJX Alloys (Implants) - Corrosion UCS | - Cascade Neural Network + RF | - Zn, Mn, Sr, Ca content - UCS - Corrosion rate | - Accuracy > 0.95 | - Compositional window proposed |
| (Zhang et al., 2024b) | - AZ80 Mg Alloy - Thermodynamic stress prediction | - TCMSSA-ELM | - Temp - Strain - Strain rate - Stress | - RMSE: 61.96% - R²: 1.43% | - Improved prediction with TCM-SSA |
| (Radha, 2024) | - Mg Alloy Battery Anodes Corrosion behavior | - XGBoost | - Corrosion current density - Corrosion rate | - R²: 0.9931 | - Strong correlation - Explained by Spearman & Kendall |
| (Mukunda et al., 2023) | - AZ31-MWCNT Composite - Wear resistance Corrosion | - XGBoost | - Load - Speed - MWCNT % - Wear loss - Hardness | - R²: 0.999 (train) 0.908 (test) | - Hardness with MWCNT - Less surface damage |
| (Würger et al., 2019) | - Corrosion inhibition - modeling | - ML + DFT + Molecular Dynamics | - Corrosion inhibition data - Inhibitor performance | - Virtual screening success | - Simulated new inhibitor molecules |
| (Wei et al., 2022) | - Mg Second Phases - Work function prediction | - SVR - GBT - MLR - XGBoost | - DFT data - (150 samples) - Work function | - SVR best prediction | - Predicted Mg7Zn3 phase well |
| (Wang et al., 2020) | - Al-Mg Intermetallics - Crystal structure prediction | - Deep Potential - + PSO | - Formation energy - DFT data - Stable crystal structures | - Identified ductile/hard phases | - Efficient convex hull screening |
| (Zhang et al., 2022) | - 6xxx Al-Mg-Si Alloys - Corrosion morphology | - CNN - + Fractal analysis | - Corrosion images - Morphology match - with field data | - CNN >70% match with field images | - Identified acidified tests as a best fit |

Table SM13 Cluster 7: Data-driven design and optimization techniques

| Ref. | Alloy System / Material Focus | ML Technique/ Optimization Approach | Target Properties | Validation Method | Key Findings/ Contribution |
| --- | --- | --- | --- | --- | --- |
| (Ling et al., 2024) | - Binary Mg alloys (Mg-Ca, Mg-Zn, etc.) | - XGB - Feature-based Screening | - Cell voltage - Specific energy - Capacity - Efficiency | - SEM - PDP curves - Hydrogen evolution | - Identified top 5 anode materials - Mg-Ca showed highest specific energy |
| (Çolak, 2025) | - High-entropy Mg-Y-Ni-Cu | - ANN | - Discharge capacity - Potential - Retention ratio | - Prediction accuracy (0.26% deviation) | - ML reduces trial cost - Optimized energy storage alloys |
| (Liu et al., 2025a) | - Mg alloy fracturing balls | - Multi-objective ML with GA | - Corrosion rate - Compressive strength | - Train/Test split accuracy (0.98/0.93) | - Designed Mg-6.4Al-3.4Zn-4.6Cu with optimized strength/corrosion |
| (Cheng et al., 2025) | - Bulk Metallic Glasses (Zr-Cu-Al-Ag) | - Stacking Ensemble - SHAP - Bayesian Optimization (BOA) | - Glass-Forming Ability (GFA) | - R2 score (0.79) - SHAP analysis | - Revealed formation law - Verified MLS in Cu-Mg-Ca alloys |
| (Ouyang et al., 2025) | - Mg-Gd based alloys | - ML-integrated design - Composition optimization | - Creep resistance | - Literature review - and discussion | - Guidelines for creep-resistant Mg alloys using ML |
| (El-Sanabary et al., 2024) | - Mg-Zn-Ca alloys (ECAP-processed) | - Regression models - ANOVA - DOE - GA - MOGA | - Wear behavior - (VL, COF) | - Wear testing - XRD - Response surfaces | - Optimized ECAP process for wear resistance using ML |
| (Singh et al., 2024) | - Spray-coated AZ91D Mg alloys | - ASO-RF - (Seagull Optimization +RF) - Parameter tuning | - Attrition loss | - Prediction performance comparison | - Optimized coating conditions for wear resistance |
| (Maqbool et al., 2024) | - WE43 Mg alloy (FSP-processed) | - ML + Virtual Sample Generation (PSO) - DOE - Sensitivity Analysis | - Corrosion rate | - GUI - SHAP analysis | - Created GUI to predict corrosion - Highlighted shoulder diameter impact |
| (Wang et al., 2023b) | - Mg-Al-Ca-Mn (AXM100) | - SVR - Hot-processing map-based optimization | - Flow behavior - DRX kinetics - Strength-Ductility | - Experimental validation - DRX analysis | - SVR improved prediction accuracy - Identified optimal extrusion parameters |
| (Li et al., 2024b) | - Al Li alloys | - Compositional ML model - Virtual search space & compositional optimization | - Specific modulus - Tensile strength | - Experimental Validation of 6 alloys | - 0.96 wt.% Ga alloy showed best performance - Solid solubility & microstructure considered |
| (Dong et al., 2023) | - Mg-based binary and ternary alloys | - GBR (Ab_max) - MLP (De_max) - SHAP - Descriptor-based screening | - Hydrogen absorption and release | - R2 scores (0.947, 0.922) - SHAP interpretation | - Identified high-performing hydrogen storage alloys (e.g., 96Mg-4Sm) |
| (Zhang et al., 2021) | - Precipitation- strengthened Cu alloys | - Correlation screening + Bayesian Optimization - Iterative alloy design | - Hardness (HV) - Electrical conductivity (EC) | - Experimental validation | - Designed Cu-Ni-Co-Si-Mg alloy with superior combined HV and EC |
| (Gupta et al., 2021) | - A380 Al alloy (Pressure die casting) | - Fuzzy Logic Methodology (FLM), - Taguchi DOE + GA | - Casting defects (flash, cold-shut, porosity) | - Regression analysis - ANOVA - R² validation | - Reduced defects through optimized PDC parameters using FLM-GA |
| (Jafari et al., 2015) | - L-bending Al sheet metal | - ANFIS + Teaching Learning Based Optimization - Taguchi DOE + FE model validation | - Springback - minimization | - FE simulation - Experimental validation | - ANFIS model successfully predicted and minimized springback |
| (Shimanek et al., 2022) | - Ni-based and Mg-based alloys | - Correlation analysis - Atomic descriptor screening | - Ideal shear strength | - First-principles calculations | - Identified atomic - properties influencing shear strength - Useful for ML applications |
| (Song et al., 2019) | - 7075-T6 Al / AZ31B Mg (FSW) | - BPNN + Gray Wolf Optimization (GWOA) - Hybrid AI optimization | - Tensile shear load | - Experimental validation (9.05 kN load) | - Optimized joint strength 11.8% higher than previous - Hybrid AI model - effective |

Table SM14. Actionable AI strategies and deployment challenges across key Mg alloy application domains

| Application Domain | Recommended AI Strategy | Deployment Challenge | Proposed Solution |
| --- | --- | --- | --- |
| Automotive Alloys | CNN for image-based strength prediction | Generalization across casting routes | Data augmentation + transfer learning |
| Biomedical Implants | RF for biodegradation rate prediction | Model interpretability | SHAP + multi-output regression |
| High-Temp Alloys | GNNs for phase stability | Training data scarcity | Physics-informed generative models |
| Corrosion Simulation | Ensemble models for multi-factor interaction | Dynamic environmental modeling | Time-series DL + feedback coupling |

A schematic representation of a CNN framework trained to predict tensile strength from electron backscatter diffraction (EBSD) or microstructure images is presented in Figure SM1.  This framework enables the automated extraction of features related to grain boundaries and texture patterns, thereby capturing complex structure property relationships that typically surpass the analytical capabilities of conventional methods. Such an approach facilitates more accurate and efficient characterization of material behavior directly from high-dimensional microstructural data.

Figure SM1. CNN-based microstructure-to-strength prediction workflow

The ML framework for predicting post-treatment mechanical properties from thermal parameters namely, solutionizing temperature, aging time, and cooling rate is depicted in Figure SM2. The developed model effectively captures the complex nonlinear interactions induced by heat treatment on hardness, strength, and ductility.

Figure SM2.  ML-based prediction framework for heat treatment effects on mechanical properties in Mg alloys

The SHAP summary plot illustrates the relative contributions of individual features toward predicting the biodegradation rates of magnesium-based implants, as depicted in Figure SM3. The analysis indicates that higher concentrations of Zn and Ca positively influence degradation rates, whereas reduced immersion times exert a detrimental effect.

Figure SM3. SHAP summary plot for biodegradation rate prediction in Mg alloys

An LSTM-based time-series model for predicting the evolution of grain size in magnesium alloys under dynamic thermal conditions is illustrated in Figure SM4. The model effectively captures temporal dependencies related to variables such as temperature, duration, and cooling rate by processing these sequential inputs, thereby addressing limitations inherent in conventional predictive approaches, particularly concerning microstructural transformation. This enables accurate forecasting of ultimate recrystallization outcomes, facilitating process optimization and precise microstructural control in magnesium alloy engineering.

Figure SM4. Time-series deep learning framework for grain growth prediction in Mg alloys

Figure SM5 illustrates a data-driven optimization framework combining experimental data, simulation outputs, and literature sources with machine learning and optimization algorithms. The workflow predicts alloy properties and recommends optimal compositions and processing parameters. This closed-loop system supports efficient exploration of design space, accelerating the development of high-performance magnesium alloys for structural and biomedical applications.

Figure SM5. Data-driven optimization workflow for Mg alloy design

References

Álvarez-Zapatero, P., Vega, A., and Aguado, A. (2021). A neural network potential for searching the atomic structures of pure and mixed nanoparticles. Application to ZnMg nanoalloys with an eye on their anticorrosive properties. Acta Materialia 220. doi: 10.1016/j.actamat.2021.117341.

Anne, G., Bhat, N., Vishwanatha, H.M., Ramesh, S., Maruthi Prashanth, B.H., Sharma, P., et al. (2024). Effect of addition of Ce and accumulative roll bonding on structure-property of the Mg-Ce-Al hybrid composite and its prediction and comparison using artificial neural network (ANN) approach. Materials Research Express 11(9). doi: 10.1088/2053-1591/ad7449.

Athul, A.S., Muthachikavil, A.V., Buddhiraju, V.S., Premraj, K., and Runkana, V. (2025). Identification of Stable Intermetallic Compounds for Hydrogen Storage via Machine Learning. Energy Storage 7(1). doi: 10.1002/est2.70115.

B, S., Ramasamy, P., Vignesh R, V., and V, B. (2025). Yttrium oxide reinforced AZ31B processed by FSP: Predictive modeling of mechanical, tribological, and corrosion properties. Materials Science and Technology (United Kingdom). doi: 10.1177/02670836251316550.

Bahari-Sambran, F., Carreño, F., Cepeda-Jiménez, C.M., and Orozco-Caballero, A. (2024). Predicting grain size-dependent superplastic properties in friction stir processed ZK30 magnesium alloy with machine learning methods. Journal of Magnesium and Alloys 12(5), 1931-1943. doi: 10.1016/j.jma.2024.05.019.

Bai, M., Wu, X., Tang, S., Lin, X., Yang, Y., Cao, L., et al. (2024). Study on hot deformation behavior and recrystallization mechanism of an Al-6.3Zn-2.5Mg-2.6Cu-0.11Zr alloy based on machine learning. Journal of Alloys and Compounds 1000. doi: 10.1016/j.jallcom.2024.175086.

Batalović, K., Radaković, J., Paskaš Mamula, B., Kuzmanović, B., and Medić Ilić, M. (2022). Predicting the Heat of Hydride Formation by Graph Neural Network - Exploring the Structure–Property Relation for Metal Hydrides. Advanced Theory and Simulations 5(9). doi: 10.1002/adts.202200293.

Byun, S., Yu, J., Cheon, S., Lee, S.H., Park, S.H., and Lee, T. (2024). Enhanced prediction of anisotropic deformation behavior using machine learning with data augmentation. Journal of Magnesium and Alloys 12(1), 186-196. doi: 10.1016/j.jma.2023.12.007.

Chandana, K.S., and Kamesh, R. (2024). Machine learning insights into prediction of H2 gravimetric capacity in Mg-based pure metal alloys. International Journal of Hydrogen Energy 77, 695-711. doi: 10.1016/j.ijhydene.2024.06.186.

Chen, K.X., Wang, Y., Dong, Y.Q., Zhao, Z.H., Zang, Y., Zhang, G.L., et al. (2025). Theoretical design of dual-site metallo-covalent organic frameworks for efficient CO2 photoreduction into C2H4. Applied Catalysis B: Environmental 365. doi: 10.1016/j.apcatb.2024.124933.

Chen, T., Gao, Q., Yuan, Y., Li, T., Xi, Q., Liu, T., et al. (2022a). Coupling physics in machine learning to investigate the solution behavior of binary Mg alloys. Journal of Magnesium and Alloys 10(10), 2817-2832. doi: 10.1016/j.jma.2021.06.014.

Chen, T., Yuan, Y., Mi, X., Wu, J., Tang, A., Wang, J., et al. (2022b). Interaction of elements in dilute Mg alloys: A DFT and machine learning study. Journal of Materials Research and Technology 21, 4512-4525. doi: 10.1016/j.jmrt.2022.11.071.

Chen, W., Gou, W., Li, Y., Li, X., Li, M., Hou, J., et al. (2024a). Machine learning design of 400 MPa grade biodegradable Zn-Mn based alloys with appropriate corrosion rates. International Journal of Minerals, Metallurgy and Materials 31(12), 2727-2736. doi: 10.1007/s12613-024-2995-4.

Chen, Y., Li, Q., Chen, X., Tan, J., and He, H. (2024b). Simulation of recrystallization grain growth in AZ61 magnesium alloy based on GA and 3D CA. Materials Letters 377. doi: 10.1016/j.matlet.2024.137452.

Chen, Y., Tian, Y., Zhou, Y., Fang, D., Ding, X., Sun, J., et al. (2020). Machine learning assisted multi-objective optimization for materials processing parameters: A case study in Mg alloy. Journal of Alloys and Compounds 844. doi: 10.1016/j.jallcom.2020.156159.

Cheng, D.J., Liang, Y.C., Pu, Y.W., and Chen, Q. (2025). Ensemble learning predicts glass-forming ability under imbalanced datasets. Computational Materials Science 248. doi: 10.1016/j.commatsci.2024.113601.

Cheng, S., Li, Z., Zhang, H., Yan, X., and Chu, S. (2024). Discovery of magnesium-aluminum alloys by generative model and automatic differentiation approach. Modelling and Simulation in Materials Science and Engineering 32(4). doi: 10.1088/1361-651X/ad38d0.

Choudhuri, D. (2021). Local structure and bonding environment of intermetallic β1 precipitate phase nucleus in binary Mg-Nd. Computational Materials Science 187. doi: 10.1016/j.commatsci.2020.110111.

Çolak, A.B. (2025). An innovative study on high entropy energy storage mg-Y-Ni-cu systems: Machine learning-driven optimization of electrical cycling in Ni-MH battery alloys. Journal of Energy Storage 107. doi: 10.1016/j.est.2024.114958.

Dai, J., Yang, J., Zhang, X., Zhang, L., Sun, B., Li, X., et al. (2024). Synergistic effects of BSA adsorption and shear stress on corrosion behaviors of WE43 alloy under simulated physiological flow field. Corrosion Science 237. doi: 10.1016/j.corsci.2024.112317.

Dargusch, M., Wang, Y., Sha, C., Yang, N., Chen, X., Venezuela, J., et al. (2024). Insights into heat treatments of biodegradable Mg-Y-Nd-Zr alloys in clinical settings: Unveiling roles of β' and β1 nanophases and latent in vivo hydrogen evolution. Acta Biomaterialia 190, 605-622. doi: 10.1016/j.actbio.2024.10.047.

Davydzenka, T., Sinclair, D., Chawla, N., and Tahmasebi, P. (2022). Deep-layers-assisted machine learning for accurate image segmentation of complex materials. Materials Characterization 192. doi: 10.1016/j.matchar.2022.112175.

Deng, J. (2024). Large-Scale Atomistic Simulations of Magnesium Oxide Exsolution Driven by Machine Learning Potentials: Implications for the Early Geodynamo. Geophysical Research Letters 51(16). doi: 10.1029/2024GL109793.

Díaz-Romero, D., Van den Eynde, S., Zaplana, I., Zhou, C., Sterkens, W., Goedemé, T., et al. (2023). Classification of aluminum scrap by laser induced breakdown spectroscopy (LIBS) and RGB + D image fusion using deep learning approaches. Resources, Conservation and Recycling 190. doi: 10.1016/j.resconrec.2023.106865.

Dong, S., Wang, Y., Li, J., Li, Y., Wang, L., and Zhang, J. (2023). Exploration and design of Mg alloys for hydrogen storage with supervised machine learning. International Journal of Hydrogen Energy 48(97), 38412-38424. doi: 10.1016/j.ijhydene.2023.06.108.

Efa, D.A. (2024). Computational modeling and virtual analysis using a moving heat source to join AZ61A and AA7075 alloys with the application of a titanium alloy interlayer. Infrared Physics and Technology 141. doi: 10.1016/j.infrared.2024.105501.

El-Garaihy, W.H., Alateyah, A.I., Alawad, M.O., Alsunaydih, F.N., El-Sanabary, S., El-Asfoury, M.S., et al. (2024). Optimization of ECAP parameters of ZX30 alloy using feature engineering assisted machine learning and response surface approaches. Materials Today Communications 40. doi: 10.1016/j.mtcomm.2024.109560.

El-Sanabary, S., Kouta, H., Shaban, M., Alrumayh, A., Alateyah, A.I., Alsunaydih, F.N., et al. (2024). A comparative study of machine learning and response surface methodologies for optimizing wear parameters of ECAP-processed ZX30 alloy. Heliyon 10(13). doi: 10.1016/j.heliyon.2024.e33967.

Fang, Z., Wang, S., Fan, H., Zhao, X., Ji, H., Li, B., et al. (2025). Machine-learning-assisted catalytic performance predictions of binary alloy catalysts for glucose hydrogenation. Applied Catalysis A: General 691. doi: 10.1016/j.apcata.2024.120086.

Farooq, M.Z., Wu, Y., Zheng, M., and Lu, L. (2025). Ignition-proof magnesium alloys with rare earth elements: A novel framework to predict combustion phases, surface morphologies, and hidden features using heating rates. Journal of Magnesium and Alloys. doi: 10.1016/j.jma.2025.01.014.

Feng, T., and Lu, G. (2024). Hydration MgCl2-NaCl-KCl molten salt using a novel approach for training machine learning potential. Journal of Molecular Liquids 394. doi: 10.1016/j.molliq.2023.123533.

Feng, X., Wang, Z., Jiang, L., Zhao, F., and Zhang, Z. (2023). Simultaneous enhancement in mechanical and corrosion properties of Al-Mg-Si alloys using machine learning. Journal of Materials Science and Technology 167, 1-13. doi: 10.1016/j.jmst.2023.04.072.

Feng, Y., Tian, Y., Yang, Y., Zhang, Y., Guo, H., and Li, J. (2024). Analyze the Performance of Electroactive Anticorrosion Coating of Medical Magnesium Alloy Using Deep Learning. Computers, Materials and Continua 79(1), 263-278. doi: 10.32604/cmc.2024.047004.

Gao, T., Zhan, Z., Hu, W., and Meng, Q. (2024). A novel damage mechanics and XGBoost based approach for HCF life prediction of cast magnesium alloy considering internal defect characteristics. International Journal of Fatigue 182. doi: 10.1016/j.ijfatigue.2024.108220.

Geng, X., Wang, L.W., and Meng, X. (2025). Exploring the strength-concentration relationship of MgCu bioalloys at low copper content using machine learning force fields. Computational Materials Science 246. doi: 10.1016/j.commatsci.2024.113486.

Ghorbani, M., Boley, M., Nakashima, P.N.H., and Birbilis, N. (2023). A machine learning approach for accelerated design of magnesium alloys. Part B: Regression and property prediction. Journal of Magnesium and Alloys 11(11), 4197-4205. doi: 10.1016/j.jma.2023.09.010.

Ghorbani, M., Boley, M., Nakashima, P.N.H., and Birbilis, N. (2024). An active machine learning approach for optimal design of magnesium alloys using Bayesian optimisation. Scientific Reports 14(1). doi: 10.1038/s41598-024-59100-9.

Gu, J., Jiang, S., Guo, W., Wang, L., and Zhang, J. (2024). An improved extreme learning machine model for predicting the mechanical property of AZ80 magnesium alloy. Applied Physics A: Materials Science and Processing 130(8). doi: 10.1007/s00339-024-07740-z.

Gupta, A.K., Kumar, S., Chandna, P., and Bhushan, G. (2021). Optimization of Process Parameters during Pressure Die Casting of A380: a Silicon-Based Aluminium Alloy Using GA & Fuzzy Methodology. Silicon 13(8), 2429-2443. doi: 10.1007/s12633-020-00594-z.

Gurugubelli, S., Chintada, V.B., and Chekuri, R.B.R. (2023). Investigation on Mechanical Properties of Fabricated Aluminium 5000 Series using Finite Element and Artificial Intelligence Methods. International Journal of Vehicle Structures and Systems 15(2), 183-186. doi: 10.4273/ijvss.15.2.07.

He, X., Liu, J., Yang, C., and Jiang, G. (2023). Predicting thermodynamic stability of magnesium alloys in machine learning. Computational Materials Science 223. doi: 10.1016/j.commatsci.2023.112111.

Huang, S.J., Sanjaya, J., Adityawardhana, Y., and Kannaiyan, S. (2024). Enhancing the Mechanical Properties of AM60B Magnesium Alloys through Graphene Addition: Characterization and Regression Analysis. Materials 17(18). doi: 10.3390/ma17184673.

Jaafreh, R., Kang, Y.S., and Hamad, K. (2023). Brittle and ductile characteristics of intermetallic compounds in magnesium alloys: A large-scale screening guided by machine learning. Journal of Magnesium and Alloys 11(1), 392-404. doi: 10.1016/j.jma.2022.05.006.

Jaafreh, R., Kim, J.G., and Hamad, K. (2022). Interpretable Machine Learning Analysis of Stress Concentration in Magnesium: An Insight beyond the Black Box of Predictive Modeling. Crystals 12(9). doi: 10.3390/cryst12091247.

Jafari, M., Lotfi, M., Ghaseminejad, P., Roodi, M., and Teimouria, R. (2015). Numerical control and optimization of springback in L-bending of magnesium alloy through FE analysis and artificial intelligence. Transactions of the Indian Institute of Metals 68(5), 969-979. doi: 10.1007/s12666-015-0535-7.

Jagadeesh, G.V., and Setti, S.G. (2023). Tribological Characterization of Ball Burnished Magnesium Alloy by Wear-Burnishing Maps, Wear Maps and Artificial Intelligence Technique. Arabian Journal for Science and Engineering 48(3), 3111-3131. doi: 10.1007/s13369-022-07025-8.

Jain, S., Bhowmik, A., and Lee, J. (2025a). Machine learning approaches for predicting and validating mechanical properties of Mg rare earth alloys for light weight applications. Science and Technology of Advanced Materials 26(1). doi: 10.1080/14686996.2025.2449811.

Jain, S., Jain, R., Dewangan, S., and Bhowmik, A. (2024). A Machine learning perspective on hardness prediction in multicomponent Al-Mg based lightweight alloys. Materials Letters 365. doi: 10.1016/j.matlet.2024.136473.

Jain, S., Jain, R., Patel, M., Sahoo, B., and Bhowmik, A. (2025b). Harnessing machine learning for predicting mechanical properties of lightweight Mg alloys. Materials Letters 378. doi: 10.1016/j.matlet.2024.137597.

Ji, Y., Fu, X., Ding, F., Xu, Y., He, Y., Ao, M., et al. (2024). Artificial intelligence combined with high-throughput calculations to improve the corrosion resistance of AlMgZn alloy. Corrosion Science 233. doi: 10.1016/j.corsci.2024.112062.

Jiang, L., Fu, H., Zhang, Z., Zhang, H., Zhang, X., Feng, X., et al. (2024a). Synchronously enhancing the strength, toughness, and stress corrosion resistance of high-end aluminum alloys via interpretable machine learning. Acta Materialia 270. doi: 10.1016/j.actamat.2024.119873.

Jiang, L., Wang, C., Fu, H., Shen, J., Zhang, Z., and Xie, J. (2022). Discovery of aluminum alloys with ultra-strength and high-toughness via a property-oriented design strategy. Journal of Materials Science and Technology 98, 33-43. doi: 10.1016/j.jmst.2021.05.011.

Jiang, Q., Jia, Z., Lu, S., Song, P., Gao, Z., Wang, Z., et al. (2024b). Novel NLi4-BGra/MgH2-based heterojunctions for efficient hydrogen storage and modulation of hydrogen-desorption temperature ranges. Ceramics International 50(13), 23058-23069. doi: 10.1016/j.ceramint.2024.04.028.

Jiang, W., Zhang, Y., Zhang, L., and Wang, H. (2021). Accurate Deep Potential model for the Al-Cu-Mg alloy in the full concentration space. Chinese Physics B 30(5). doi: 10.1088/1674-1056/abf134.

Juan, Y., Niu, G., Yang, Y., Dai, Y., Yang, J., and Zhang, J. (2024). Machine learning-based identification method of new strengthening element and the study on Al-Zn-Mg-Cu-Zr-Hf alloy. Materials Today Communications 38. doi: 10.1016/j.mtcomm.2024.108359.

Kim, T., Ryu, W.H., Yoo, G.H., Park, D., Kim, J.Y., Park, E.S., et al. (2024). Data-driven discovery of ultrahigh specific hardness alloys. Journal of Materials Research and Technology 33, 7753-7760. doi: 10.1016/j.jmrt.2024.11.153.

Kuriki, D., Briffod, F., Shiraiwa, T., and Enoki, M. (2024). Multimodal deep learning framework to predict strain localization of Mg/LPSO two-phase alloys. Acta Materialia 281. doi: 10.1016/j.actamat.2024.120398.

Li, C., Zhang, H., Guo, D., and Zeng, W. (2024a). Crystal Structure Prediction and Property Calculation of Al2CuMg by Deep Learning Potential. Journal of Materials Engineering and Performance 33(24), 13721-13730. doi: 10.1007/s11665-023-08944-9.

Li, G., Cheng, L., Yue, Q., Hu, X., Lu, H., and Zhu, Q. (2023). Predicting temperature of semi-solid 7075 aluminum alloy slurry prepared by a novel rheocasting route via neural network. Materials Letters 349. doi: 10.1016/j.matlet.2023.134753.

Li, H., Li, X., Li, Y., Gao, G., Wen, K., Li, Z., et al. (2024b). Exploration of Alloying Elements of High Specific Modulus Al–Li Alloy Based on Machine Learning. Materials 17(1). doi: 10.3390/ma17010092.

Li, K.Y., Liu, L.C., Shao, L.L., Zhou, J., Ke, H.B., Li, M.Z., et al. (2025). Generative model-based inverse design of Fe-based metallic glasses with high saturation magnetic flux density. Journal of Alloys and Compounds 1010. doi: 10.1016/j.jallcom.2024.178325.

Li, M., Mesbah, M., Fallahpour, A., Nasiri-Tabrizi, B., and Liu, B. (2021). Mechanical strength estimation of ultrafine-grained magnesium implant by neural-based predictive machine learning. Materials Letters 305. doi: 10.1016/j.matlet.2021.130627.

Li, S., Liu, R., Yan, H., Li, Z., Li, Y., Li, X., et al. (2024c). Machine Learning Phase Prediction of Light-Weight High-Entropy Alloys Containing Aluminum, Magnesium, and Lithium. Metals 14(4). doi: 10.3390/met14040400.

Li, X., Liu, Y., Luan, S., Ma, D., Liu, X., Liu, Q., et al. (2024d). Investigation of deformation behavior of Mg-2Ho alloy based on hyperbolic sine constitutive equation and PSO-BP neural network. Materials Today Communications 38. doi: 10.1016/j.mtcomm.2023.107613.

Liang, T., Yuan, Y., Chen, T., Wang, J., Zhang, L., Wu, L., et al. (2024). Electrical conductivity of binary magnesium alloys: Integrating first-principles and machine learning studies. Materials Today Communications 40. doi: 10.1016/j.mtcomm.2024.110021.

Ling, N., Wang, Y., Song, S., Liu, C., Yang, F., Qi, X., et al. (2024). Experimentally validated screening strategy for alloys as anode in Mg-air battery with multi-target machine learning predictions. Chemical Engineering Journal 496. doi: 10.1016/j.cej.2024.153824.

Liu, Q., Wu, H., Paul, M.J., He, P., Peng, Z., Gludovatz, B., et al. (2020). Machine-learning assisted laser powder bed fusion process optimization for AlSi10Mg: New microstructure description indices and fracture mechanisms. Acta Materialia 201, 316-328. doi: 10.1016/j.actamat.2020.10.010.

Liu, X., Yang, J., Yi, L., Li, D., Wang, Q., Du, H., et al. (2025a). Multi-objective optimization of fracturing ball strength and corrosion rate with genetic algorithms and interpretable machine learning. Advanced Composites and Hybrid Materials 8(1). doi: 10.1007/s42114-024-01199-5.

Liu, Z., Xiao, Y., Yang, L., Liu, W., Yan, G., Sun, Y., et al. (2025b). Failure prediction of thermal barrier coatings on turbine blades under calcium-magnesium-alumina-silicate corrosion and thermal shock. Acta Mechanica Sinica/Lixue Xuebao 41(5). doi: 10.1007/s10409-024-24285-x.

Lopes Marinho, A., Kazimi, B., Ćwieka, H., Marek, R., Beckmann, F., Willumeit-Römer, R., et al. (2024). A comparison of deep learning segmentation models for synchrotron radiation based tomograms of biodegradable bone implants. Frontiers in Physics 12. doi: 10.3389/fphy.2024.1257512.

Ma, S., Zhang, D., Zhang, P., and Markert, B. (2025). Rapid prediction of the corrosion behaviour of coated biodegradable magnesium alloys using phase field simulation and machine learning. Computational Materials Science 247. doi: 10.1016/j.commatsci.2024.113546.

Ma, S., Zhang, Z., Huang, Z., Song, D., Jia, Y., Zhou, N., et al. (2022). Prediction of Grain Size in Cast Aluminum Alloys. Crystals 12(4). doi: 10.3390/cryst12040474.

Maqbool, A., Khalad, A., and Khan, N.Z. (2024). Prediction of corrosion rate for friction stir processed WE43 alloy by combining PSO-based virtual sample generation and machine learning. Journal of Magnesium and Alloys 12(4), 1518-1528. doi: 10.1016/j.jma.2024.04.012.

Masood Chaudry, U., Hamad, K., and Abuhmed, T. (2021). Machine learning-aided design of aluminum alloys with high performance. Materials Today Communications 26. doi: 10.1016/j.mtcomm.2020.101897.

Medghalchi, S., Zubair, M., Karimi, E., Sandlöbes-Haut, S., Kerzel, U., and Korte-Kerzel, S. (2023). Determination of the Rate Dependence of Damage Formation in Metallic-Intermetallic Mg–Al–Ca Composites at Elevated Temperature using Panoramic Image Analysis. Advanced Engineering Materials 25(21). doi: 10.1002/adem.202300956.

Menon, V., Das, S., Gavini, V., and Qi, L. (2024). Atomistic simulations and machine learning of solute grain boundary segregation in Mg alloys at finite temperatures. Acta Materialia 264. doi: 10.1016/j.actamat.2023.119515.

Menze, R., Hesse, B., Kusmierczuk, M., Chen, D., Weitkamp, T., Bettink, S., et al. (2024). Synchrotron microtomography reveals insights into the degradation kinetics of bio-degradable coronary magnesium scaffolds. Bioactive Materials 32, 1-11. doi: 10.1016/j.bioactmat.2023.09.008.

Messina, J., Luo, R., Xu, K., Lu, G., Deng, H., Tschopp, M.A., et al. (2021). Machine learning to predict aluminum segregation to magnesium grain boundaries. Scripta Materialia 204. doi: 10.1016/j.scriptamat.2021.114150.

Mi, X., Dai, L., Jing, X., She, J., Holmedal, B., Tang, A., et al. (2024). Accelerated design of high-performance Mg-Mn-based magnesium alloys based on novel bayesian optimization. Journal of Magnesium and Alloys 12(2), 750-766. doi: 10.1016/j.jma.2024.01.005.

Mishra, A. (2024a). Artificial intelligence algorithms for prediction of the ultimate tensile strength of the friction stir welded magnesium alloys. International Journal on Interactive Design and Manufacturing 18(3), 1779-1787. doi: 10.1007/s12008-022-01180-w.

Mishra, A. (2024b). Data driven knowledge summarization of friction stir welded magnesium alloys literature by using natural language processing algorithms. International Journal on Interactive Design and Manufacturing 18(3), 1113-1119. doi: 10.1007/s12008-022-01118-2.

Mo, W., Xiao, Y., Huang, Y., Sun, P., Li, Y., Zheng, X., et al. (2025). Active learning-based alloy design strategy for improving the strength-ductility balance of Al-Mg-Zn alloys. Materials and Design 252. doi: 10.1016/j.matdes.2025.113772.

Mokhtari, M.A., Nikzad, M.H., and Jalalvand, M. (2024). Competition of systematically optimized deep neural networks for the estimation of tensile behavior of aluminum-magnesium alloy. Physica Scripta 99(6). doi: 10.1088/1402-4896/ad4218.

Mondal, S., Samanta, R., Shit, S., Biswas, A., Bandyopadhyay, A., Dhar, R.S., et al. (2024). CORROSION PREDICTION OF MAGNESIUM IMPLANT USING MULTISCALE MODELING BASED ON MACHINE LEARNING ALGORITHMS. International Journal for Multiscale Computational Engineering 22(4), 125-141. doi: 10.1615/IntJMultCompEng.2023050288.

Motamedi, M., Nikzad, M.H., and Nasri, M.R. (2023). Mixture design optimization and machine learning-based prediction of Al-Mg alloy composite reinforced by Zn nanoparticles: A molecular dynamics study. Materials Today Communications 37. doi: 10.1016/j.mtcomm.2023.107473.

Mukunda, S.G., Srivastava, A., Boppana, S.B., Dayanand, S., and Yeshwanth, D. (2023). Wear Performance Prediction of MWCNT-Reinforced AZ31 Composite Using Machine Learning Technique. Journal of Bio- and Tribo-Corrosion 9(2). doi: 10.1007/s40735-023-00745-w.

Murugesan, M., Yu, J.H., Chung, W., and Lee, C.W. (2023). Hybrid Artificial Neural Network-Based Models to Investigate Deformation Behavior of AZ31B Magnesium Alloy at Warm Tensile Deformation. Materials 16(15). doi: 10.3390/ma16155308.

Nithin, A.M., Davidson, M.J., and Rao, C.S.P. (2022). Effect of Various Mg/Si Ratios on Microstructure and Structural Properties of Thixoextruded Al-Si-Mg Alloys. Silicon 14(17), 11675-11686. doi: 10.1007/s12633-022-01689-5.

Österreicher, J.A., Živanović, D., Walenta, W., Maimone, S., Hofbauer, M., Hovden, S., et al. (2024). In situ conductometry for studying the homogenization of Al-Mg-Si alloys and predicting extrudate grain structure through machine learning. Materials and Design 243. doi: 10.1016/j.matdes.2024.113070.

Otieno, R., Odhong, E.V., and Ondieki, C. (2024). Prediction of phases and mechanical properties of magnesium-based high-entropy alloys using machine learning. Journal of King Saud University - Science 36(10). doi: 10.1016/j.jksus.2024.103456.

Ouyang, S., Wu, Q., Kim, R.E., Lee, J.H., Lee, J.A., and Kim, H.S. (2025). Recent Progress in Developing Creep-Resistant Mg-Gd-Based Alloys. Metals and Materials International. doi: 10.1007/s12540-025-01918-7.

Pagadala, N.D., jaiswal, J., and R, R. (2023). Machine learning based corrosion prediction of as cast Mg-Sn alloys for biomedical applications. Materials Today Communications 35. doi: 10.1016/j.mtcomm.2023.106108.

Pei, S., Dai, C., Yang, X., Zhang, L., Wang, H., Zhang, S., et al. (2024a). Quantitative prediction of Mg-RE-Ni alloy corrosion behavior by machine learning. Corrosion Science 237. doi: 10.1016/j.corsci.2024.112324.

Pei, Y., Li, L., Yu, M., Wei, E., Zhao, M., and Teng, B. (2024b). Comparison and evaluation of different constitutive models for predicting the hot deformation behavior of Mg-Gd-Y-Zr alloy. Journal of Magnesium and Alloys. doi: 10.1016/j.jma.2024.08.004.

Pei, Z., and Yin, J. (2019). Machine learning as a contributor to physics: Understanding Mg alloys. Materials and Design 172. doi: 10.1016/j.matdes.2019.107759.

Peng, Q., Yuan, X., Zhao, S., Zhou, Y., Wen, X., and Chen, X.J. (2023). Active-learning search for unitcell structures: A case study on Mg3Bi2-xSbx. Computational Materials Science 226. doi: 10.1016/j.commatsci.2023.112260.

Qi, X., Liu, A., Li, Y., Dang, L., Zhang, J., and Wang, L. (2025). Deep learning and finite element simulation of spatiotemporal multiscale fusion: Real time prediction of magnesium alloys corrosion covered with MAO coatings. Materials Today Communications 44. doi: 10.1016/j.mtcomm.2025.111915.

Radha, R. (2024). Predicting corrosion current density in magnesium alloy battery anodes: machine learning approach using rapid miner. Canadian Metallurgical Quarterly. doi: 10.1080/00084433.2024.2425497.

Raguraman, S., Priyadarshini, M.S., Nguyen, T., McGovern, R., Kim, A., Griebel, A.J., et al. (2024). Machine learning-guided accelerated discovery of structure-property correlations in lean magnesium alloys for biomedical applications. Journal of Magnesium and Alloys 12(6), 2267-2283. doi: 10.1016/j.jma.2024.06.008.

Rahnama, A., and Sridhar, S. (2019). Application of data science tools to determine feature correlation and cluster metal hydrides for hydrogen storage. Materialia 7. doi: 10.1016/j.mtla.2019.100366.

Shaban, M., Alateyah, A.I., Alsharekh, M.F., Alawad, M.O., BaQais, A., Kamel, M., et al. (2023). Influence of ECAP Parameters on the Structural, Electrochemical and Mechanical Behavior of ZK30: A Combination of Experimental and Machine Learning Approaches. Journal of Manufacturing and Materials Processing 7(2). doi: 10.3390/jmmp7020052.

Shimanek, J.D., Shang, S.L., Beese, A.M., and Liu, Z.K. (2022). Insight into ideal shear strength of Ni-based dilute alloys using first-principles calculations and correlational analysis. Computational Materials Science 212. doi: 10.1016/j.commatsci.2022.111564.

Shu, C., He, J., Xue, G., and Xie, C. (2022). Grain Knowledge Graph Representation Learning: A New Paradigm for Microstructure-Property Prediction. Crystals 12(2). doi: 10.3390/cryst12020280.

Singh, A., Agarwal, T., Gambhir, V., and Harinaiha, A. (2024). Estimation of Attrition Loss Due to Spray-On Coatings for Mg Alloys Using a Novel Machine Learning Approach. Nanotechnology Perceptions 20(S3), 291-303. doi: 10.62441/nano-ntp.v20iS3.22.

Song, Q., Ren, Z., Ji, S., Niu, S., Qi, W., and Chen, M. (2019). Improving the Mechanical Property of Dissimilar Al/Mg Zn-Added Ultrasound-Assisted Friction Stir Lap Welding Joint by Back Propagation Neural Network–Gray Wolf Optimization Algorithm. Advanced Engineering Materials 21(12). doi: 10.1002/adem.201900973.

Suh, J.S., Suh, B.C., Bae, J.H., and Kim, Y.M. (2023). Machine learning-based design of biodegradable Mg alloys for load-bearing implants. Materials and Design 225. doi: 10.1016/j.matdes.2022.111442.

Suh, J.S., Suh, B.C., Lee, S.E., Bae, J.H., and Moon, B.G. (2022). Quantitative analysis of mechanical properties associated with aging treatment and microstructure in Mg-Al-Zn alloys through machine learning. Journal of Materials Science and Technology 107, 52-63. doi: 10.1016/j.jmst.2021.07.045.

Sun, X., and Liu, B. (2023). A learning-based optimal uncertainty quantification method and its application to ballistic impact problems. Mechanics of Materials 184. doi: 10.1016/j.mechmat.2023.104727.

Tian, L., and Yu, W. (2021). Effects of cluster expansion on the locations of phase transition boundary as a first step to quantify uncertainty in first principles statistical mechanics framework. Computational Materials Science 186. doi: 10.1016/j.commatsci.2020.110050.

Troncoso, J.F., Hu, Y., della Ventura, N.M., Sharma, A., Maeder, X., and Turlo, V. (2023). Machine learning of twin/matrix interfaces from local stress field. Computational Materials Science 228. doi: 10.1016/j.commatsci.2023.112322.

Wang, H., Duan, Z., Guo, Q., Zhang, Y., and Zhao, Y. (2023a). Machine Learning Design of Aluminum-Lithium Alloys with High Strength. Computers, Materials and Continua 77, 1393-1409. doi: 10.32604/cmc.2023.045871.

Wang, H., Zhang, Y., Zhang, L., and Wang, H. (2020). Crystal Structure Prediction of Binary Alloys via Deep Potential. Frontiers in Chemistry 8. doi: 10.3389/fchem.2020.589795.

Wang, M., Yu, H.L., Chen, Y., and Huang, M.X. (2021). Machine learning assisted screening of non-rare-earth elements for Mg alloys with low stacking fault energy. Computational Materials Science 196. doi: 10.1016/j.commatsci.2021.110544.

Wang, Q., Qin, X., Xia, S., Wang, L., Wang, W., Huang, W., et al. (2025). Interpretable machine learning excavates a low-alloyed magnesium alloy with strength-ductility synergy based on data augmentation and reconstruction. Journal of Magnesium and Alloys. doi: 10.1016/j.jma.2025.01.003.

Wang, Q., Zhai, H., Jin, Z., He, J., Yang, Q., Liu, W., et al. (2023b). Hot-deformation kinetics analysis and extrusion parameter optimization of a dilute rare-earth free magnesium alloy. Journal of Magnesium and Alloys 11(9), 3302-3322. doi: 10.1016/j.jma.2022.07.013.

Wang, S., Wu, Y., Xu, Q., Ma, Y., and Wang, T. (2024a). Research on stamping formability and process simulation of AZ31 magnesium alloy based on deep learning. Materials Today Communications 40. doi: 10.1016/j.mtcomm.2024.109807.

Wang, Y., Tang, Q., Xu, X., Weng, P., Ying, T., Yang, Y., et al. (2023c). Accelerated discovery of magnesium intermetallic compounds with sluggish corrosion cathodic reactions through active learning and DFT calculations. Acta Materialia 255. doi: 10.1016/j.actamat.2023.119063.

Wang, Y., Xie, T., Tang, Q., Wang, M., Ying, T., Zhu, H., et al. (2024b). High-throughput calculations combining machine learning to investigate the corrosion properties of binary Mg alloys. Journal of Magnesium and Alloys 12(4), 1406-1418. doi: 10.1016/j.jma.2021.12.007.

Wei, X., Wang, J., Wang, C., Zhu, S., Wang, L., and Guan, S. (2022). Prediction of electronic work function of the second phase in binary magnesium alloy based on machine learning method. Journal of Materials Research 37(21), 3792-3802. doi: 10.1557/s43578-022-00752-6.

Wiese, B., Berger, S., Bohlen, J., Nienaber, M., and Höche, D. (2023). Property design of extruded magnesium-gadolinium alloys through machine learning. Materials Today Communications 36. doi: 10.1016/j.mtcomm.2023.106566.

Wu, H., Chen, X., Yang, L., Zheng, D., Zhou, J., Zhang, E., et al. (2025a). Mechanism study of rare earth Y enhancing A356 tensile performance: Deep learning potential and Ab initio molecular dynamics. Materials Today Communications 44. doi: 10.1016/j.mtcomm.2025.111868.

Wu, Y., Snihirova, D., Würger, T., Wang, L., Feiler, C., Höche, D., et al. (2025b). Machine learning-guided discovery of high-efficiency electrolyte additives for aqueous magnesium-air batteries. Energy Storage Materials 76. doi: 10.1016/j.ensm.2025.104120.

Würger, T., Feiler, C., Musil, F., Feldbauer, G.B.V., Höche, D., Lamaka, S.V., et al. (2019). Data science based mg corrosion engineering. Frontiers in Materials 6, 1-9. doi: 10.3389/fmats.2019.00053.

Xue, D., Wei, W., Shi, W., Zhou, X., Rong, L., Wen, S., et al. (2022). Microstructural evolution and constitutive analysis of Al-Mg-Zn-Er-Zr based on arrhenius-type and machine-learning algorithm. Materials Today Communications 32. doi: 10.1016/j.mtcomm.2022.104076.

Xue, D., Wei, W., Shi, W., Zhou, X.R., Qi, J.T., Wen, S.P., et al. (2023). Optimization of stabilized annealing of Al-Mg alloys utilizing machine learning algorithms. Materials Today Communications 35. doi: 10.1016/j.mtcomm.2023.106177.

Yadav, P.K., and Khurana, M.K. (2022). Experimental investigation and optimization of quality characteristics during friction stir welding of Al- and Zn-based magnesium alloy using artificial intelligence. Proceedings of the Institution of Mechanical Engineers, Part L: Journal of Materials: Design and Applications 236(2), 345-360. doi: 10.1177/14644207211044805.

Yanase, Y., Miyauchi, H., Matsumoto, H., and Yokota, K. (2022). Densification Behavior and Microstructures of the Al-10%Si-0.35Mg Alloy Fabricated by Selective Laser Melting: From Experimental Observation to Machine Learning. Materials Transactions 63(2), 176-184. doi: 10.2320/matertrans.MT-M2021215.

Yang, W., Wang, Y., Huang, X., Liu, S., Wang, P., and Du, Y. (2024). Effects of Cu content and Sintering temperature on microstructure and mechanical properties of SiCp/Al-Cu-Mg composites through experimental study, CALPHAD-type simulation and machine learning. Journal of Materials Research and Technology 33, 2216-2225. doi: 10.1016/j.jmrt.2024.09.202.

Yu, J., Lee, S.H., Cheon, S., Park, S.H., and Lee, T. (2024). Alternative predictive approach for low-cycle fatigue life based on machine learning and energy-based modeling. Journal of Magnesium and Alloys 12(10), 4075-4084. doi: 10.1016/j.jma.2024.10.014.

Zhang, C., Zhang, Y., Ren, B., Wu, Y., Hu, Y., Chai, Y., et al. (2025a). Accelerated design of age-hardened Mg-Ca-Zn alloys with enhanced mechanical properties via machine learning. Computational Materials Science 249. doi: 10.1016/j.commatsci.2025.113665.

Zhang, D., Srinivasan, J., and Locke, J.S. (2022). Quantitative Evaluation of the Ability of Accelerated Tests to Simulate On-Road Corrosion Morphology of Automotive Aluminum Alloys. Corrosion 78(12), 1229-1249. doi: 10.5006/4174.

Zhang, G., Mei, W., Zhang, W., and Yu, K. (2025b). Exploring the mechanism of plastic deformation in BCC Mg-Li-Al alloys via Machine learning Molecular dynamics simulations. Computational Materials Science 246. doi: 10.1016/j.commatsci.2024.113396.

Zhang, H., Fu, H., Li, W., Jiang, L., Yong, W., Sun, J., et al. (2024a). Empowering the Sustainable Development of High-End Alloys via Interpretive Machine Learning. Advanced Materials 36(48). doi: 10.1002/adma.202404478.

Zhang, H., Fu, H., Zhu, S., Yong, W., and Xie, J. (2021). Machine learning assisted composition effective design for precipitation strengthened copper alloys. Acta Materialia 215. doi: 10.1016/j.actamat.2021.117118.

Zhang, P., Zhang, J., Fu, J., Guo, W., Zhao, D., and Wang, L. (2024b). Property prediction of AZ80 magnesium alloy: an extreme learning machine model optimized by a new improved sparrow search algorithm. Revista Materia 29(3). doi: 10.1590/1517-7076-RMAT-2024-0296.

Zhang, S., Yi, W., Zhong, J., Gao, J., Lu, Z., and Zhang, L. (2023a). Computer Alloy Design of Ti Modified Al-Si-Mg-Sr Casting Alloys for Achieving Simultaneous Enhancement in Strength and Ductility. Materials 16(1). doi: 10.3390/ma16010306.

Zhang, X., Wang, A., Shao, C., and Bao, H. (2024c). Understanding thermal transport in magnesium solid solutions through first-principles approaches and machine learning feature screening. Acta Materialia 276. doi: 10.1016/j.actamat.2024.120160.

Zhang, Y., Bai, S., Jiang, B., Li, K., Dong, Z., and Pan, F. (2023b). Modeling the correlation between texture characteristics and tensile properties of AZ31 magnesium alloy based on the artificial neural networks. Journal of Materials Research and Technology 24, 5286-5297. doi: 10.1016/j.jmrt.2023.04.079.

Zhang, Y., Tu, X., Deng, A., Wu, D., Hu, Y., Yan, B., et al. (2025c). Machine learning-assisted design of filler for laser welding of Al-Zn-Mg-Cu alloy. Materials Letters 383. doi: 10.1016/j.matlet.2025.137974.

Zhang, Y., Wang, N., Li, J., Mesbah, M., Wong, K.Y., Fallahpour, A., et al. (2020). Mechanical properties modeling of severely plastically deformed biodegradable zk60 magnesium alloy for bone implants. Latin American Journal of Solids and Structures 17(5), 1-23. doi: 10.1590/1679-78256151.

Zhu, G., Du, X., and Sun, D. (2025a). Machine learning accelerated design of magnesium alloys with high strength and high ductility. Materials Today Communications 44. doi: 10.1016/j.mtcomm.2025.111894.

Zhu, Y., Cao, Y., Peng, L., Yu, Q., Yang, Z., Li, Z., et al. (2025b). Design of a novel Cu-Cr-X alloy with high strength and high electrical conductivity based on mechanical learning. Materials and Design 250. doi: 10.1016/j.matdes.2025.113599.