Green synthesis of carbon nanospheres from Vachellia nilotica for pendimethalin removal

Krupal Vidhyarthi1†, Gautam Priyadarshi2†, Bhakti Patel2, Santosh Kumar Sahu, Esha Rami1*, Dipak Kumar Sahoo3*, and Ashish Patel2*

1 Department of Life Sciences, Parul Institute of Applied Science, Parul University, Vadodara-391760, Gujarat, India; krupal5456@gmail.com (K.V.)

2 Department of Life Sciences, Hemchandracharya North Gujarat University, Patan-384265, Gujarat, India; priyadarshigautam411@gmail.com (G.P.); bhaktipatel2233@gmail.com (B.P.); santoshsahu.hngu@gmail.com (S.K.S)

3 Department of Veterinary Clinical Sciences, College of Veterinary Medicine, Iowa State University, Ames, Iowa, USA

† These authors contributed equally and share the first authorship

*Corresponding authors: esha.rami82036@paruluniversity.ac.in (E.R.);

dsahoo@iastate.edu (D.K.S.); uni.ashish@gmail.com (A.P.)

Supplementary Material

Table S1. Physico-chemical properties of PND.

| Property | Value |
| --- | --- |
| Molecular formula | C₁₃H₁₉N₃O₄ |
| IUPAC Name | N-(1-ethylpropyl)-2,6-dinitro-3,4-xylidine |
| Molecular weight | 281.31 g/mol |
| CAS number | 40487-42-1 |
| Sructure |  |
| Appearance | Yellow-orange crystals/powder |
| Melting point | Yellow-orange crystals/powder |
| Boiling point | 54 to 60 °C |
| Solubility in water (25 at °C) | 0.3 to 0.54 mg/L(insoluble) |
| Solubility in organic solvents | Very soluble (acetone, methanol, xylene, etc.) |
| pKa (25 at °C) | 2.8 |
| log Kow | 5.2 |
| Half-life in soil | ~90 days |
| Vapor Pressure | 3.3 × 10⁻⁵ mmHg at 25 °C (low volatility) |

Table S2. Liner and non-liner expression of adsorption kinetics and isotherm models.

| Model | Linear form | Non-linear form | Parameters / Notes |
| --- | --- | --- | --- |
| Pseudo-first order (PFO) | logqe- qt=logqe- K12.303t | qt=qe1-e-k1.t | adsorption capacity qe (mg g-1) and qt (mg g-1) and K1 is rate constant. |
| Pseudo-second order (PSO) | tqt=1k2qe2+ tqe | qt=qe2k2tqek2t+1 | k2 is pseudo second-order rate constant (g/mg·min) |
| Intraparticle diffusion (IPD) | qe=C+Kidt1/2 | same as linear form | kid is intraparticle diffusion rate constant (mg/g·min^0.5) and C is the intercept related to boundary level thickness. |
| Langmuir isotherm | ceqe=1qmKL+ceqm | qe=qm. KL.Ce1+KL.Ce | qm = maximum amount of adsorbent, Ce = model constant, KL= adsorption equilibrium constant. |
| Freundlich isotherm | log qe=logKf+1nlog Ce | qe=KF.Ce1/n | Kf = adsorption capacity n= adsorption intensity |
| Temkin isotherm | qe=RTBTlnKT+RTBTlnce | qe=BT×ln(KTce) | B = Temkin constant, RT/BT= heat of adsorption, R= gas constant T= temperature (K) |

Table S3 Cost analysis for preparation of CNSs.

| Description of item required for |  | Unit cost (INR) | No. of Units | Price (INR) |
| --- | --- | --- | --- | --- |
| 1 | Biomass | 0 | 0 | 0 |
| 2 | Electricity |  |  | 39.6978 |
|  | - Microwave irradiation (800 W for 3 min) | 5.2 per KWh | 0.04 KWh | 0.21 |
|  | - Muffle furnace (3000 W for 2.5 hours) | 5.2 per KWh | 7.5 kWh | 39 |
|  | - Ultrasonication (170 W for 30 minute) | 5.2 per KWh | 0.085 kWh | 0.442 |
|  | - Vortex (55 W for 10 min) | 5.2 per KWh | 0.0092 kWh | 0.048 |
| 3 | Chemicals |  |  |  |
|  | - ferrocene | 550 per 25 gm | 0.150 g (150 mg) | 3.30 |
|  | - ethanol | 140 per 500 mL | 100 mL (assumed) | 28 |
| 4 | Distilled Water | 20 Rs per L | 1 L | 20 |
| Total (per batch) |  |  |  | 90.998 |

Approximate 91 (INR) was required to synthesize 200 mg of CNSs. Therefore, the cost of CNSs per gram will be 455 INR (~$5.45/g).

Figure S1. pHZPC of CNSs using pH drift method.

Figure S2. Comparative PND removal efficiency at 50 mg L-1 concentration, 7 pH, 100 ml volume and 100 mg CNS and VNBC dose.

Figure S3. FEG-SEM image of VNBC at 25000x magnification.