Supplementary Material

The correlation of adsorption behavior between ciprofloxacin hydrochloride and the active sites of Fe-doped MCM-41

Ying Wu, Yiming Tang*, Laisheng Li, Peihong Liu, Xukai Li, Weirui Chen, Ying Xue

* Correspondence: Yiming Tang: y.tang@m.scnu.edu.cn

# Supplementary Figures and Tables

## Supplementary Figures

Supplementary Figure S1. TEM images of pure MCM-41 (A) and Fe-MCM-41(20) (B).

Supplementary Figure S2. FT-IR spectra of CPX, Fe-MCM-41 and CPX-adsorbed Fe-MCM-41over the range 4000-400 cm-1.

## Supplementary Tables

Supplementary Table S1. Structural properties of adsorbents.

| Sample | SBET (m2 g-1) | Pore diameter (nm) | Pore Volume (cm3 g-1) |
| --- | --- | --- | --- |
| MCM-41 | 1002.1 | 3.2 | 0.79 |
| Fe-MCM-41 (160) | 894.7 | 3.5 | 0.79 |
| Fe-MCM-41 (80) | 883.2 | 3.6 | 0.80 |
| Fe-MCM-41 (40) | 822.6 | 3.8 | 0.79 |
| Fe-MCM-41 (20) | 625.6 | 4.3 | 0.68 |