Supplementary Material

1  Supplementary Figures

FIGURE S1│The geometries of original h-BN (A), optimized primitive cell porous BN (p-BN) (B), and supercell 221 p-BN (C), respectively.

FIGURE S2│The cohesive energies of isolated Aun cluster, Aun/p-BN-VN (n=2~13) and Au bulk.

FIGURE S3│Potential energy diagrams for the migration of a single Au atom on VN vacancy.

FIGURE S4│Total density of states (TDOS) for p-BN with VB defect (A) and p-BN with VN defect (B).

FIGURE S5│The total charge density of p-BN with VB defect (A) and p-BN with VN defect (B).

FIGURE S6│ The charge-density difference plots of O2 adsorbed on Au/p-BN-VN: (A) *O2-Bridge, (B) *O2-Pauling.

FIGURE S7│The geometry structures of H2O2 adsorption on Au/p-BN-VN, Pt13 and Au13 cluster.

FIGURE S8│The structures for initial state (IS), transition state (TS), final state (FS) and potential energy profile for (A) *O2→ *O + *O, (B) *OOH → *OH + *O on a Au atom supported p-BN with VN.

FIGURE S9│The structures for initial state (IS), transition state (TS), final state (FS) and potential energy profile for (A) *O2→ *O + *O, (B) *OOH + H+ + e- → H2O2* on Au13 cluster.

FIGURE S10│The possible reaction pathways for ORR on Au/p-BN-VN surface. The * denotes the adsorption site on the Au/p-BN-VN surface. The values (in units of eV) represent the activation energy. The paths with the blue sign is the most favorable due to their lower activation energies.

2  Supplementary Tables

Table S1│ The adsorption energies (Eads, eV), O-O lengths, and charges transfer amount from catalysts to O2 obtained by the Hirshfeld Charge analysis of the adsorbed *O2-Bridge on metal (Pt, Pd, and Au)/p-BN with B and N vacancy defect.

| Catalysts | Eads O2 (eV) | dO-O (Å) | dM-O (Å) | Charge (e) |
| --- | --- | --- | --- | --- |
| Pt/p-BN-VB | 1.043 | 1.312 | 2.016 | 0.202 |
| Pt/p-BN-VN | 2.213 | 1.347 | 2.141 | 0.230 |
| Pd/p-BN-VB | 0.611 | 1.302 | 2.070 | 0.205 |
| Pd/p-BN-VN | 1.976 | 1.336 | 2.070 | 0.343 |
| Au/p-BN-VB | 0.522 | 1.280 | 2.008 | 0.128 |
| Au/p-BN-VN | 1.658 | 1.489 | 1.979 | 0.513 |

Table. S2│ The calculated adsorption energies (Eads/eV) of *O2, *OOH, *O, *OH and H2O on Au/p-BN-VN, which obtained in a H2O solvent environment by COSMO.

|  | O2 (Bridge) | O2(Pauling) | OOH | OH | O | H2O |
| --- | --- | --- | --- | --- | --- | --- |
| Eads/eV | 1.658 | 0.717 | 1.925 | 3.282 | 5.413 | 0.488 |
| Eads/eV(COSOM) | 2.031 | 1.150 | 1.911 | 3.274 | 5.752 | 0.509 |