Magnetic solid phase extraction based on nanostructured magnetic porous porphyrin organic polymer for simultaneous extraction and preconcentration of neonicotinoid insecticides from surface water

Shirley K. Selahle1,2, Ngwako J. Waleng1,2, Anele Mpupa1.2, Philiswa N. Nomngongo1,2,3

1 Department of Chemical Sciences, University of Johannesburg, Doornfontein Campus, P.O. Box 17011, Doornfontein, 2028, South Africa

2DSI/NRF SARChI Chair: Nanotechnology for Water, University of Johannesburg, Doornfontein 2028, South Africa.

3DSI/Mintek Nanotechnology Innovation Centre, University of Johannesburg, Doornfontein 2028, South Africa

Supplementary Material

# Supplementary Figures and Tables

## Supplementary Tables

Table S1: Independent variable and their levels used in design of experiments (DOE)

| Variable | Minimum | Central | Maximum |
| --- | --- | --- | --- |
| Mass of adsorbent (mg) | 20 | 25 | 50 |
| pH | 4 | 6.5 | 9 |
| Extraction time (min) | 10 | 15 | 20 |
| Eluent volume (µL) | 100 | 550 | 1000 |

Table S2: Factorial design matrix and the respective analytical responses

| Standard Run |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | MA | EV | pH | ET | Clothi | Imida | Aceta | Thia |
| 1 | 20 | 100 | 4 | 10 | 43,6 | 23,9 | 28,4 | 31,3 |
| 2 | 50 | 100 | 4 | 20 | 18,4 | 16,4 | 17,3 | 20,7 |
| 3 | 20 | 1000 | 4 | 20 | 88,9 | 65,4 | 74,7 | 78,1 |
| 4 | 50 | 1000 | 4 | 10 | 67,2 | 36,6 | 43,1 | 42,9 |
| 5 | 20 | 100 | 9 | 20 | 37,8 | 47,9 | 55,1 | 46,3 |
| 6 | 50 | 100 | 9 | 10 | 48,6 | 20,5 | 27,6 | 23,3 |
| 7 | 20 | 1000 | 9 | 10 | 78,8 | 45,2 | 51,0 | 53,2 |
| 8 | 50 | 1000 | 9 | 20 | 78,0 | 40,2 | 44,2 | 52,9 |
| 9 (C) | 35 | 550 | 7 | 15 | 82,0 | 72,0 | 81,7 | 83,7 |
| 10 (C) | 35 | 550 | 7 | 15 | 84,6 | 68,4 | 84,2 | 85,5 |
| 11 (C) | 35 | 550 | 7 | 15 | 82,1 | 72,4 | 83,8 | 85,3 |
| 12 (C) | 35 | 550 | 7 | 15 | 82,2 | 69,1 | 87,0 | 87,8 |

Table S3: Central composite design matrix and the respective analytical responses.

| Expt | Mass of adsorbent | Eluent volume | Extr. time | %R |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Aceta | Chlothia | Imida | Thia |
| 1 | 20.0 | 100 | 10 | 55.5 | 26.0 | 32.7 | 35.7 |
| 2 | 20.0 | 100 | 20 | 76.6 | 69.7 | 80.3 | 92.6 |
| 3 | 20.0 | 1000 | 10 | 103.0 | 95.0 | 102.1 | 97.8 |
| 4 | 20.0 | 1000 | 20 | 87.8 | 100.3 | 89.3 | 97.3 |
| 5 | 50.0 | 100 | 10 | 66.1 | 55.1 | 63.5 | 86.1 |
| 6 | 50.0 | 100 | 20 | 98.2 | 92.5 | 106.3 | 95.8 |
| 7 | 50.0 | 1000 | 10 | 95.5 | 100.7 | 79.9 | 70.6 |
| 8 | 50.0 | 1000 | 20 | 78.3 | 84.4 | 97.6 | 80.2 |
| 9 | 15.7 | 550 | 15 | 26.4 | 24.7 | 27.6 | 32.2 |
| 10 | 54.0 | 550 | 15 | 40.2 | 58.0 | 18.2 | 31.7 |
| 11 | 35.0 | -29 | 15 | 0.0 | 0.0 | 0.0 | 0.0 |
| 12 | 35.0 | 1129 | 15 | 83.4 | 82.1 | 82.1 | 99.0 |
| 13 | 35.0 | 550 | 8.6 | 69.5 | 65.5 | 65.5 | 73.2 |
| 14 | 35.0 | 550 | 21 | 70.0 | 81.8 | 81.8 | 81.5 |
| 15 (C | 35.0 | 550 | 15 | 96.2 | 97.8 | 97.8 | 94.9 |
| 16 (C) | 35.0 | 550 | 15 | 96.1 | 101.5 | 101.5 | 97.4 |

Table S4 Physicochemical properties of neonicotinoid insecticides and their EF values on the MP-POP adsorbent

| Compound name | Structures | Molecular mass (g/mol) | LogKowa | EF | H bond acceptor | H bond donors |
| --- | --- | --- | --- | --- | --- | --- |
| Acetamiprid |  | 222.67 | 0.8 | 98 | 4 | 0 |
| Imidacloprid |  | 255.661 | 0.6 | 94 | 5 | 1 |
| Clothianidin |  | 249.678 | 0.7 | 104 | 5 | 2 |
| Thiacloprid |  | 252.72 | 1.3 | 110 | 4 | 0 |

a Data adopted from

## Supplementary Figures

Figure S1. Pareto charts of standardised effect for preconcentration of (a) acetamiprid, (b) clothianadin, (c) imidacloprid and (d) thiacloprid. EV = Eluent volume; MA= Mass of adsorbent; ET=; Extraction time, 1 by 2= interaction of mass and the eluent volume; 1by3 = interaction of mass of adsorbent and pH; 1 by 4 = Interaction of mass of the adsorbent and extraction time;

Figure S2. Response surface methodology 3D surface plots showing interaction effects.

Figure S3. Profile for predicted values and desirability

A

B

Figure S4 Effect initial concentration and sample volume

Figure S5. Chromatogram of acetamiprid (Aceta), imidacloprid (Imida), Clothiandin (Clothia) and Thiacloprid (Thia) from river water sample spiked with 100 ng L−1 of each analyte.

Figure S6. Typical chromatogram obtained after application of UA-DMSPE/HPLC-DAD method for analysis of river water sample 1. Acetamiprid (Aceta), imidacloprid (Imida), Clothiandin (Clothia) and Thiacloprid (Thia)

Figure S7. Regeneration and reusability of MP-POP. Acetamiprid (Aceta), imidacloprid (Imida), Clothiandin (Clothia) and Thiacloprid (Thia). Experimental conditions: sample volume, 30 mL; mass of the adsorbent, 15 mg; acetonitrile volume, 1130 µL; time of desorption, 5 min; extraction time, 15 min and pH of sample, 7.0.

Corresponding author: E-mail address:pnnomngongo@uj.ac.za, Tel: +27115596187