Trimetallic NiVCe-LDH as multifunctional nanomaterials for supercapacitor, oxygen evolution reaction, and sensor applications

Josué M. Gonçalves1*, Irlan S. Lima1, Nathália F. B. Azeredo1, Diego P. Rocha1, Abner de Siervo2 and Lúcio Angnes1*

1Instituto de Química, Universidade de São Paulo, Av. Prof. Lineu Prestes 748, 05508-000, São Paulo-SP, Brazil.

2Institute of Physics “Gleb Wataghin”, Applied Physics Department, State University of Campinas, 13083-859, Campinas-SP, Brazil.

Corresponding authors: josuemartins@usp.br (JMG) and luangnes@iq.usp.br (LA)

Figure S1. X-ray diffractograms of (A) Ni0.9V0.1-LDH and (B) Ni0.8V0.1Ce0.1-LDH NPs deposited on a glass slip substrate.

Figure S2. XPS survey spectrum showing the characteristic elements presented for the synthesis of LDH NPs.

Figure S3. High-resolution XPS from samples synthesized with a single element. (A) Ni 2p from Ni(OH)2 nanoparticles. (B) V 2p, consistent with nanoparticles in the V2O5 phase. (C) Ce 3d consistent with Ce(OH)2 NPs of pure Ce3+ phase.

Figure S4. TEM images of Ce(OH)3 deposited on graphene oxide (GO) sheets.

Figure S5. High-resolution XPS for Ce 3d and Ni 2p core levels from samples Ni0.8V0.1Ce0.1-LDH.  The attempt to fit the peak structure, especially in the Ce 3d region demonstrates that extra structures are present, suggesting the LDH formation.

Figure S6. Hydrodynamic voltammetric recordings acquired in the optimization of the  working potential in the presence of 10 mmol L-1 H2O2 on the Ni0.9V0.05Ce0.05-LDH SPE after electrochemical activation with NaOH 0.5 mol L-1. Background electrolyte: KCl 0.1 mol L-1.

Figure S7. Optimization of the volume (red) and dispensing speed (black) in BIA technique in the presence of 10 mmol L-1 H2O2 on the Ni0.9V0.05Ce0.05-LDH SPE after electrochemical activation with NaOH 0.5 mol L-1. Background electrolyte: KCl 0.1 mol L-1.