Supplementary Material

## Supplementary Table

|  | Coating Parameters A020 | Coating Parameters A021 |  |
| --- | --- | --- | --- |
| Matrix | NOA73 | NOA73 |  |
| Graphene | 2% w/w | 2% w/w |  |
| Zinc | 5% w/w | - |  |
| Mixing | Magnetic stirring 5 min | Magnetic stirring 5 min |  |
| Spray pressure | 1.7 bar | 1.7 bar |  |
| Number of spray passes | 2 horizontal, 2 verticals | 2 horizontal, 2 verticals |  |
| Nozzle size | 0.5 mm | 0.5 mm |  |
| Curing | 150C for 12h | 150C for 12h |  |
| Characterization | A020 | A021 |
| Visual aspect | Uniform | Uniform |
| Thickness | 9.9 µm | 8.7 µm |
| Adhesion | Class 0 | Class 0 |
| NSSt | No sign of corrosion, the coating integrity is maintained. Precipitation of ZnO powder | No sign of corrosion, the coating integrity is maintained. |
| Resistance | 1.1Ω to 1.8 Ω | 5kΩ |

Supplementary Table s1. Parameters and results for the A020 and A021 coatings.

## Supplementary Figures

Supplementary Figure s1. NOA73 coating loaded with 1% w/w graphene.

Supplementary Figure s2. LEXT roughness profile for the A020 coating.

Supplementary Figure s3. LEXT roughness profile for the A021 coating.